BUREAU OF INDIAN STANDARDS

SUMMER INTERNSHIP REPORT

DURATION: 05 May, 2025 – 27 June, 2025

LOCATION: BIS Headquarter, New Delhi

Submitted By:

Subhodipa De,

National Institute of Technology, Durgapur.

Submitted To:

Shri. HAWELIKAR DUSHYANT SATYAPREM

Scientist – C/DD, MTD

BIS – HQ

TABLE OF CONTENTS

- Acknowledgement …………………………………………………………….03

Chapter No. 1 BLACK OXIDE COATING [Black_Oxide_Coating]

  - Indian Standards (IS) under consideration …….……………………………...04

  - Need For Revision of Standards……………………………………………….05

  - Literature Survey Report Details………………………………………………07

  - International Standards available………………………………………………15

  - Comparative study of different International Standards……………………….16

  - Recommendation……………………………………………………………….18

  - Draft…………………………………………………………………………….18

  - References………………………………………………………………………18

Chapter No. 2 ZINC ELECTROPLATING [Zinc_Electroplating]

  - Indian Standards (IS) under consideration ……………...………………………19

  - Literature Survey Report Details………………………………………………...19

  - International Standards available………………………………………………...27

  - Comparative study of different International Standards…………………………28

  - Recommendation…………………………………………………………………34

  - Draft………………………………………………………………………………34

  - References………………………………………………………………………...35

Industry Survey Report [Industry_DeepakFastenersLtd] ……………………………….36

ACKNOWLEDGEMENT

I would like to thank Bureau of Indian Standards, HQ for giving me this opportunity to do my internship in the organization.

I would also like to express my sincere gratitude to my guide, Hawelikar Dushyant Satyaprem, Scientist - C, Metallurgical Engineering Department, Bureau of Indian Standards, Head Quarter, New Delhi, for his invaluable support and guidance throughout this project. Dushyant sir’s expertise, insightful feedback, and constant encouragement have been instrumental in shaping this work and enhancing its quality.

I am particularly grateful for the time Dushyant sir dedicated to reviewing my work, providing constructive criticism, and suggesting improvements that have undoubtedly elevated the standard of this project. His mentorship has guided this project and instilled in me a deeper appreciation for scientific inquiry and rigorous methodology.

The completion of this study would not have been possible without Dushyant sir’s unwavering support and guidance. His contributions to my internship journey at BIS Head Quarters, New Delhi have been truly exceptional, and I am profoundly thankful for his mentorship.

SUBHODIPA DE

BLACK OXIDE COATING

INDIAN STANDARDS (IS) UNDER CONSIDERATION

Indian Standards, developed by the Bureau of Indian Standards (BIS), guarantee effectiveness, safety, and quality in a range of industries. These standards include management system standards, test procedures, codes of conduct, and product standards. This thorough analysis covers every kind of standard, elaborating on their meaning and structure with particular instances.

The following are some examples of Indian standards; for each, the standard's content and structure are provided, along with a test report analysis for that standard revision.

- PRODUCT STANDARD: IS 13212:1991 (Reaffirmed 2021) – Black oxide coating for Iron and Steel parts – Specification

STRUCTURE:

- Scope – This standard specifies the requirements of black oxide coating (also known as chemical blackening) on iron and steel parts. Black oxide finish is unsuitable for humid, corrosive environments, non-ferrous assemblies, or areas trapping blackening chemicals. This coating shall be applied after all machining, forming, welding, cold straightening and heat-treatment processes.

- References – IS 11826: 1986[Recommended Practice for Chemical Colouring for Engineering Components in General and for Bicycle Components]

- General Requirement– Iron and Steel parts

- Coating Requirement– Black oxide coating shall meet the requirements depending on the test that shall be carried out before the application of preservative oil or after degreasing.

    - Freedom from Defects: The coating must be uniformly black, free from untreated patches, flakes, scratches, pits, and residues that could cause corrosion or degrade the organic finish.

    - Visual Tests: There shall be no indication of any reddish brown or green smut when inspected visually under strong light. The sample shall also be wiped with a clean white cloth for indication of smut.

    - Quality of Oxide Coating (Oxalic Acid Test): Three drops of 5 percent oxalic acid is deposited on black oxide coated surface. The reaction shall be observed up to 8 minutes. After 8 minutes the surface shall be rinsed and compared to a light grey centre with a light border colour indicates a poor quality coating. A grey black centre with a light border indicates a border line quality coating. A black or dark brown centre with a light border indicates good quality coating.

- Hydrogen Embrittlement– High strength steel parts having an ultimate tensile strength of 1647 N/mm2 and above shall be baked at 191+14°C for more than three hours after application of the oxide coating for embrittlement relief.

- SampIing–

- SampIing for Production Control: For quality control, sample components from bath areas likely to produce lighter shades and test them using methods as specified.

- Sampling for Acceptance of a Lot: The lot is divided into sub-lots of 100 items; two samples from each sub-lot are selected and tested as specified.

- Criteria of Acceptance: If initial samples fail, two more are tested; the sub-lot is accepted if both pass, but rejected if either fails

- Marking– The coated articles may be marked with the name or trade mark.

- PRODUCT STANDARD: IS 13147:1991 (Reaffirmed 2021) – Black oxide coating on Stainless Steel parts – Specification

STRUCTURE:

- Scope – This standard specifies the requirements for the black oxide coating on stainless steel parts.

- References – IS 11826: 1986[Recommended Practice for Chemical Colouring for Engineering Components in General and for Bicycle Components]

& 9844: 1981[Method of testing corrosion resistance of electroplated and anodized aluminium coatings by neutral salt spray test]

- General Requirement– Stainless Steel parts

- Coating Requirement– Black oxide coating shall meet the requirements depending on the test that shall be carried out before the application of preservative oil or after degreasing.

    - Freedom from Defects: The coating must be uniform with glossy black to dull black appearance depending on the condition of the basis metal and it shall cover the basis metal completely without any voids or breaks.

    - Visual Tests: There shall be no indication of any reddish brown or green smut when inspected visually under strong light.

    - Corrosion Test: Processed parts are washed in distilled water, dried with a soft cloth and then subjected to 5%salt-spray for a period of 96 hours. When tested as per IS 9844:1981, parts shall exhibit no signs of base metal corrosion after the test.

    - Quality of Oxide Coating (Oxalic Acid Test): Three drops of 5 percent oxalic acid is deposited on black oxide coated surface. The reaction shall be observed up to 8 minutes. After 8 minutes the surface shall be rinsed and compared to a light grey centre with a light border colour indicates a poor quality coating. A grey black centre with a light border indicates a border line quality coating. A black or dark brown centre with a light border indicates good quality coating.

- Sampling–

- Sampling for Production Control: For quality control, sample components from bath areas likely to produce lighter shades and test them using methods as specified.

- Sampling for Acceptance of a Lot: The lot is divided into sub-lots of 100 items; two samples from each sub-lot are selected and tested as specified.

- Criteria of Acceptance: If initial samples fail, two more are tested; the sub-lot is accepted if both passes, but rejected if either fails

Need for Revision of IS 13212 and IS 13147 Standards

The revision of IS 13212 and IS 13147 standards is essential to enhance their clarity, relevance, and practical applicability for modern industry requirements. Currently, these standards lack sufficient detail, which creates ambiguity and challenges for industries trying to implement them effectively. A detailed and well-structured standard is crucial for consistent quality and easier compliance.

Key reasons for revision include:

- Lack of Detailed Procedure Guidelines: The existing versions of IS 13212 and IS 13147 do not provide comprehensive instructions or procedures, making it difficult for industries to uniformly interpret and apply the standards. Elaboration on process parameters, quality checks, and inspection criteria is needed.

- Absence of Adhesion Test: One of the major gaps in the current standards is the omission of the test for adhesion. This test is critical for evaluating the strength of the bond between two surfaces, typically a coating or adhesive and a substrate. This strength is crucial for ensuring the durability and longevity of products, structures, and systems where adhesion is essential. Including such a test would ensure better assessment of coating performance.

- Absence of Coating Thickness Measurement Test: A significant limitation of the current standards is the lack of a defined test method for measuring coating thickness. Coating thickness directly impacts corrosion resistance, mechanical performance, and overall durability of coated components. Its measurement is essential to ensure uniformity, adherence to specifications, and functional reliability. Incorporating this test would enhance quality control and improve conformance to performance standards.

Updating these standards would not only promote consistency and quality in surface treatment practices but also help align them with international benchmarks and evolving industrial demands

Literature Survey Report

What is Black Oxide Coating?

Black oxide coatings are a type of chemical-conversion coating and are created through a chemical reaction between iron atoms on the substrate surface and oxidizing salts in a chemical bath. This forms a moderately integrated and well-attached layer of Fe3O4 (magnetite or black iron oxide). Additionally, the coating adds an aesthetically appealing matte black finish to parts, which is why the process is also sometimes referred to as “blackening.”

Black Oxide Compared with Other Metal Coatings

Black oxide coating is distinct from most other metal coatings in its application to parts. Unlike other finishes, such as painting and powder coating — processes that blanket the substrate with a protective layer that is at best only mildly chemically bonded to it — black oxide coatings are created through a direct chemical reaction of the surface atoms to form a closely coupled film. Black oxide is present as a distinct layer on the surface, but it transitions from oxide to metal in a progression through the thickness. As a result, it is well integrated with the metal substrate, offering a more robust and uniform finish.

Properties of Black Oxide Coatings

The physical properties of black oxide coatings are:

- Black oxide coating enhances the hardness of the outer surface. This increased hardness has value in applications in which resistance to abrasion and wear is crucial, providing a durable surface that withstands mechanical stress.

- The coating lends a lower coefficient of friction and greater scratch resistance to part surfaces.

- Beyond the functional physical enhancement of the surface, black oxide coatings also add to the aesthetics of components in the form of a matte black finish.

The thermal properties of black oxide coatings are:

- Black oxide coatings are thermally stable, which allows them to withstand elevated temperatures without loss of film integrity. This is essential in applications in which components may be exposed to heat, such as in engine components, gun barrels, or high-temperature industrial environments.

- Black oxide coatings are additionally effective at dissipating heat, compared with bare steel, as the colour increases the emissivity. This is particularly useful for components in which managing heat is crucial for optimal performance, such as in electronic devices or machinery.

Raw Materials

Base Materials (Substrates):     What Metals Can Be Black Oxide?

Black oxide coating is an ideal match for ferrous materials like steel and iron. The metals that can be treated with a black oxide finish include:

Steel: Steel, a common ferrous material, can be coated perfectly with black oxide, resulting in a strong, dark, and durable finish that enhances its natural toughness.

Stainless Steel:  Black oxide stainless steel provides a protective layer that offers corrosion protection for parts, it is not as durable or long-lasting as other forms of stainless steel surface treatment, such as electropolishing or physical vapor deposition (PVD) coatings.

Iron: With its robust nature, iron also takes well to the black oxide process, getting a stylish, protective layer in return. And it’s not just about the heavyweights.

Zinc: A black oxide coating can be applied to zinc parts to create an Ebonol Z finish. This surface treatment is commonly used for hardware, automotive parts and decorative items.

Copper: Copper, and its alloy buddies, brass and bronze, can also join the black oxide party, acquiring a classy, black sheen through a process tailored just for them.

Nickel: Like its metal counterparts, nickel can receive a black oxide treatment, enhancing its natural lustre and resistance. This process further ups the ante on its durability and aesthetic appeal.

Brass: Brass isn’t left out of the black oxide party either. This golden alloy also benefits from the protective black oxide layer, elevating its visual appeal and giving it an extra shield against corrosion and wear.

Chemicals Used:

- Sodium Hydroxide (NaOH)

- Nitrate/Nitrite salts

- Deionized Water: Deionized water is crucial in the black oxide coating process, especially during the final rinse stage, to ensure a clean and residue-free finish.

- Surfactants/Inhibitors (optional): to improve the quality and durability of the coating, especially in hot black oxide processes. These additives can enhance coating density, uniformity, and corrosion resistance.

- Sealing Oils (e.g., wax or oil)

| Chemical | Concentration Range (g/L) | Purpose |
| --- | --- | --- |
| Sodium Hydroxide (NaOH) | 500 – 650 | Base medium, drives the reaction |
| Sodium Nitrate (NaNO3) | 50 – 150 | Oxidizer (helps convert Fe → Fe3O4) |
| Sodium Nitrite (NaNO2) | 10 – 50 | Additional oxidizer |
| Water (H₂O) | Balance accordingly | Solvent |

The relevant HSN (Harmonized System of Nomenclature) codes and the import-export data for the key chemicals used in black oxide coating in India:

Import Data for Key Components used:

X- axis: Year     Y- axis: Quantity (in MTS)

Export Data for Key Components used:

X- axis: Year     Y- axis: Quantity (in MTS)

Reference made: (Other Components data were not available)

Sodium Hydroxide (HSN code 28151110)

- Flakes Of Sodium Hydroxide (NaOH) [SOLID]

Refer:  https://tradestat.commerce.gov.in/meidb/principal_commodity_wise_all_HSCode_import

Sodium Nitrite (HSN code 28341010)

Refer: https://tradestat.commerce.gov.in/meidb/principal_commodity_wise_all_HSCode_import

India is a significant exporter of NaOH and nitrate compounds, while sodium nitrite is largely imported, mainly from European and North American sources.

Testing Required for Raw Materials

- Tests Before Black Oxide Coating (Pre-Coating)

Surface Cleanliness Test

- Method: Visual inspection Test.

- Refer: ISO 11408 [Chemical conversion coatings — Black oxide coating on iron and steel — Specification and test methods]

- Purpose: Ensures no oil, grease, rust, or scale is present before coating.

- Tests After Black Oxide Coating (Post-Coating)

Visual Inspection

- Method: Naked eye inspection.

- Refer: ISO 11408 [Chemical conversion coatings — Black oxide coating on iron and steel — Specification and test methods]

- Purpose: Checks for uniformity, gloss, and absence of patchiness or discoloration.

- Purpose: Freedom from defects: Colored metal components shall be free from untreated patches, and flaky and uneven deposits, sometimes caused by sludge in the bath. They shall be free from scratches, pits and residues of the processing solution as it may initiate deterioration of the organic coating or premature corrosion.

Adhesion Test

- Method: Cross- Cut Test

- Refer: IS0 2409 [Paints and varnishes — Cross-cut test]

- Purpose: Ensures the coating is properly bonded to the surface.

Coating Thickness Measurement

- Method: Ultrasonic Thickness gauge.

- Refer: ISO 16809 [Non-destructive testing – Ultrasonic thickness measurement]

Ultrasonic thickness measurement operates on the pulse-echo principle, where high-frequency sound waves are used to determine the distance between the surface and the substrate by measuring the time delay of echoes.

Process Steps:

Couplant Application: A couplant (gel/liquid) is applied to eliminate air gaps and ensure efficient sound wave transmission.

Probe Placement: The ultrasonic transducer is placed on the coated surface.

Pulse Transmission: The transducer emits short ultrasonic pulses into the coating.

Echo Reception: The pulse reflects back from the coating–substrate interface and is received by the same transducer.

Time-of-Flight Calculation: The instrument calculates the coating thickness using the time taken for the echo to return and the known speed of sound in the coating material.

- Purpose: Ensures proper buildup.

Salt Spray Test (Corrosion Resistance)

- Refer: IS 5528/ ISO 9227 Corrosion Tests in Artificial Atmospheres-Salt Spray Tests

Colored components or sample panels shall be subjected to neutral salt spray test. The colour shall not become patchy nor any sign of corrosion shall occur within 24 hours. Slight staining or water mark may be allowed.

- Purpose: Evaluate how well a black oxide coating can prevent corrosion of the metal it protects.

Oxalic acid Test

- Refer: ISO 11408 [Chemical conversion coatings — Black oxide coating on iron and steel — Specification and test methods]

Three drops of 5 percent oxalic acid are deposited on black oxide coated surface. The reaction shall be observed up to 8 minutes. After 8 minutes the surface shall be rinsed and compared. A light grey center with a light border color indicates a poor-quality coating. A grey black center with a light border indicates a border line quality coating. A black or dark brown center with a light border indicates good quality coating.

The oxalic acid test for black oxide coatings is used to evaluate the coating's quality, integrity, and durability. It's a method to determine if the black oxide finish can withstand acid exposure without being damaged or corroded, ensuring it meets specific quality standards.

Here's a more detailed explanation:

Purpose: The test helps verify that the black oxide coating is effectively protecting the underlying metal and that it is uniform and of good quality.

How it works: An oxalic acid solution is applied to a black oxide coated part, rinsed off, and then visually inspected for any signs of attack or discoloration of the coating.

Significance: A good-quality coating will not exhibit any significant change in colour or appearance after exposure to the oxalic acid.

How Black Oxide Coating Works: Step-by-Step Process

- Cleaning the Surface
→ Remove dirt, oil, grease, rust, or dust
→ Use alkaline detergent or acid etch depending on surface condition

- Descaling / Pickling: This stage is essential if the parts exhibit rust or scale formation. The parts are soaked in acid solutions to remove oxide scales and corrosion products, ensuring a clean base metal surface.

- Immersion in Blackening Solution
→ Submerge in a hot bath (typically 285–305 °F / 140–150 °C)
→ Solution contains: Sodium Hydroxide (NaOH), Nitrates / Nitrites & Other oxidizing salts

- Chemical Reaction
→ Iron on surface reacts with oxidizing salts
→ Forms magnetite (Fe3O4) – the black oxide layer
→ Duration: 5 to 40 minutes depending on: Temperature, Solution strength, Desired finish

- Rinsing
→ Thoroughly rinse parts with clean water
→ Removes any residual chemicals

- Sealing / Post Treatment
→ Apply oil, wax, or sealant
→ Fills porous oxide layer
→ Improves corrosion resistance and durability

Result: A smooth, durable, matte black finish with enhanced corrosion protection and minimal dimensional change.

Clean the surface of the component to be black oxide coated

Flowchart:

Descaling: parts are soaked in acid solutions to remove oxide scales

Immersion in Blackening Solution

Chemical Reaction takes place: forms black oxide layer

Rinsing with clean water

Sealing

Industries Where Black Oxide is Most Commonly Used

A wide range of industries who use black oxide coatings for a variety of component applications. These applications most commonly include:

- Automotive fasteners, brackets, wheel components, brake components, trim pieces, and other automotive parts.

- Aerospace fasteners and brackets, landing gear components, avionic components, trim pieces, and more.

- Electronics connectors, contacts, housings, enclosures, and circuit board components.

- Hand tools, measurement gauges, jigs, dies, fixtures, tool holders, and other tools.

- Screws, bolts, nuts, washers, and threaded rods for industrial environments.

- Machine components, fasteners, rollers, gears, shafts, and more.

Advantages of Black Oxide

Using black oxide coating for a number of reasons:

- It offers significantly enhanced corrosion resistance for ferrous metals, protecting them from progressive oxidation and some other forms of attack.

- It can provide an attractive, uniform, matte black finish that makes it popular for decorative applications and makes it useful for functional applications in various industries.

- It contributes to improved hardness, lower friction, and wear resistance of the metal, which serves to extend the lifespan of products.

- Typically measured in millionths of inches, the coating thickness adds virtually no extra thickness to part surfaces, making it ideal for high-precision parts with tight tolerances.

- Compared to other coating methods like, electroplating or powder coating, black oxide is often more cost-effective.

Disadvantages of Black Oxide

Despite its many advantages, black oxide coatings do have some drawbacks:

- They are only generally applicable to ferrous metals, meaning metals like aluminium do not react well with the process.

- Applying black oxide coatings is somewhat labour-intensive due to the need to clean parts before the coating process and sealing the parts after.

- The sealing process is necessary to enhance corrosion resistance but adds a step to the overall coating process.

- In comparison with many other steel-finishing options such as powder coating or metal plating options, black oxide coatings are less durable and offer shorter service life in wet or acidic environments.

Different International Standards based on Black Oxide Coating:

- ISO 11408 [Chemical conversion coatings — Black oxide coating on iron and steel —Specification and test methods]

Scope: This International Standard specifies requirements for black oxide coatings on iron and steel (including cast and wrought iron, carbon steel, low alloyed steel and stainless steel). Black oxide coatings can be used to diminish friction between sliding or bearing surfaces or for decorative purposes or to reduce light reflection. Such coatings, with or without supplementary preservative treatment, may be used where a black surface is required. Only very limited corrosion protection is obtained under mildly corrosive conditions even with preservative treatment.

This International Standard does not specify requirements for the condition, finish or surface roughness of the substrate prior to black oxidizing.

- MIL DTL 13924E [Detail Specification- Coating, Oxide, Black, For Ferrous Metals]

Scope: This specification covers black oxide coatings applied to ferrous metals (carbon, low alloy, and corrosion resistant steels, and wrought iron). Black oxide coatings, with or without a supplementary preservative treatment, may be used where a black surface is required. Only very limited corrosion protection, under mildly corrosive conditions, is obtained as a result of black oxide coating. Black coatings are included in this specification with limitations. Unless contraindicated by contract, chrome-free finishes should be used in place of finishes containing hexavalent chromium, provided all performance criteria herein has been met and documented as OQE.

- AMS 2485 [Aerospace Material Specification- Coating, Black Oxide]

Scope:

Purpose: This specification covers the requirement for black oxide coatings on parts.

Application: This coating has been used typically to improve the anti- chafing and anti- friction properties of carbon and low alloy steel parts, particularly for sliding or caring surfaces, by providing a finish coating that retains an oil film, but usage is not limited to such applications.

Safety- Hazardous Materials: While the materials, methods, applications and processes described or referenced in this specification may involve the use of hazardous materials, this specification does not address the hazards which may be involved in such use. It is the sole responsibility of the user to ensure familiarity with the safe and proper use of any hazardous materials and to take necessary precautionary measures to ensure the health and safety of all personnel involved.

Comparative study of different International Standards based on Black Oxide Coating:

| Aspect | MIL-DTL-13924E (USA - Military) | ISO 11408:1999 (International) | IS 13147:1991/ 13212:1991 (India - BIS) | AMS 2485 (Aerospace) | Why These Differences Exist |
| --- | --- | --- | --- | --- | --- |
| Purpose | Suited for military Unique, employed for decorative purposes, or decrease in light reflection, corrosion protection | General-purpose industrial use | General industrial use in India | Improve anti- chafing and anti- friction properties | Based on intended application |
| Target Material | ferrous metals (carbon, low alloy, and corrosion resistant steels, and wrought iron) | Carbon steels, low alloy steels, wrought irons, cast irons. Martensitic stainless steel. | Iron, Steel & stainless steel | Carbon and low-alloy steels, | Military Standards and ISO includes more materials compared to other standards. |
| Bath Temperature | Class 1 :141- 152 ⁰C Class 2: 121+/- 5⁰C Class 3: 399-454⁰C Class 4: 121-130⁰C | 130–150°C for carbon steels, low alloy steels, wrought irons, cast irons, 115–125°C for martensitic stainless steel tempered at less than 480 °C 400-450 ⁰ C for Martensitic stainless steel tempered at 480 °C or higher | Not mentioned | Not mentioned | Similar base, but ISO and MIL include detailed variation for alloy types. |
| Procedure | Mentioned in detail | Not mentioned | Not mentioned | Mentioned | ISO and IS does not provide the procedure for carrying out Black oxide coating process. Since it is an important clause so, it should be present in all standards. |
| Stress Relief Requirement | Mandatory for >39 HRC hardness | Heat Treatment guided by ISO 9587/9588 | Required for high-strength steels | Steel parts 36 HRC or higher hardness and which have been ground or cold worked after heat treatment shall be stress relieved. | MIL and AMS are strict due to embrittlement risk in critical parts; IS only mention for high-strength steel |
| Salt Spray Testing | Required (up to 96 hours, ASTM B117) | Shall withstand 96h | 96 hours corrosion resistance (IS 13147) | Not mentioned | All standards provide equivalent data under this parameter. |
| Post-Treatment (Sealing) | Mandatory for all classes | Nothing mentioned | Not Mentioned | Required to achieve corrosion performance with suitable corrosion-preventive oil. | Post-treatment improves corrosion resistance; MIL and AMS mandate it strictly. Nothing mentioned in IS and ISO. |
| Inspection Methods | Visual test, oxalic acid test, smut test, salt spray test, hydrogen embrittlement relief test. | Visual test, Neutral salt spray test, oxalic acid test | Visual test, oxalic acid test | Oxalic acid spot test, smut test, Quality test, Surface and Intergranular attack test | Standards do not include adhesion test and coating thickness measurement test which are the two important parameter to take care. |
| Hydrogen Embrittlement Relief | Required as per guidelines | Follows ISO standards | Required (IS 13212_Especially for high strength steel) | Strict requirement; depending on hardness of parts below engineering drawing limits, relief procedures | All the standards include this clause accordingly. |
| Surface Appearance | Matte black, non-reflective | Uniform black finish | Uniform black | Uniform black, non-reflective | Surface Appearance is same |
| Environmental Focus | Strong (chrome-free, no ozone-depleting agents) | Not mentioned | Not mentioned | Not mentioned | Only MIL standard mention to use chrome-free but other standards do not mention such. |
| Referenced Standards | ASTM B117, ASTM F519, ASTMD1735, ASTM F22, AMS 2485, AMS 2759 | ISO 4519, ISO 9587, ISO 2064, ISO9588, ISO 9227 | IS 9844, IS 11826 | AS 2390, ASTM G 46 | MIL, ISO, and AMS cross-reference latest test methods and aerospace standards; IS uses national test references. |

RECOMMENDATION

  - Adoption of modified ISO 11408 with merging of IS 13212 & IS 13147

It was observed that IS 13212 is applicable to iron and steel whereas IS 13147 is applicable to stainless steel. The only difference which was found is hydrogen embrittlement of iron and steel. While studying ISO 11408 it was found that it is a comprehensive document which is applicable to iron, steel and stainless steel.

After analysing the comparison of different standards, it is recommended to adopt ISO 11408 with modifications for black oxide coatings on ferrous substrates, considering its comprehensive technical scope, updated test methods, and global applicability.

Modification of ISO 11408 ensures the standard is complete in all aspects. Modifications proposed are based on MIL DTL13924E and literature survey. Hence, it is proposed to merge IS 13212 and IS 13147 by adoption of modified ISO 11408.

This harmonization will streamline national standardization efforts, eliminate redundancy, and ensure alignment with internationally recognized coating practices and quality benchmarks.

Refer the given draft made with the recommendation made:  Annex_1

REFERENCES

Websites:

  - https://www.madearia.com/blog/what-is-black-oxide-coating/

  - https://fractory.com/black-oxide-coating-explained/

  - https://www.xometry.com/resources/machining/what-is-black-oxide/

  - https://waykenrm.com/blogs/black-oxide-coating-guide/#Applications-of-Black-Oxide-Finish-for-Precision-Machined-Projects

  - BIS website: https://www.bis.gov.in/

  - BIS Standards Portal: https://standardsbis.bsbedge.com/

ZINC ELECTROPLATING

INDIAN STANDARDS (IS) UNDER CONSIDERATION

Indian Standards, developed by the Bureau of Indian Standards (BIS), guarantee effectiveness, safety, and quality in a range of industries. These standards include management system standards, test procedures, codes of conduct, and product standards. This thorough analysis covers every kind of standard, elaborating on their meaning and structure with particular instances.

The following are some examples of Indian standards; for each, the standard's content and structure are provided, along with a test report analysis for that standard revision.

- PRODUCT STANDARD: IS 1573:1986 (Reaffirmed 2021) – Specification for Electroplated Coatings of Zinc on Iron and Steel

Scope: 1.1This standard covers requirements for electrodeposited zinc coatings applied to iron or steel articles except for coatings applied to components having threads of basic major diameter from 1.25 to 12.5 mm and coatings applied to sheet or wire in the unfabricated form or to close-coiled springs.

1.2 Requirements are specified for appearance, thickness, adhesion, heat treatment before or after plating, precleaning standards, and if the coating is chromate- passivated, the corrosion resistance.

- PRODUCT STANDARD: IS 6745:1972 (Reaffirmed 2021) – Methods for Determination of Mass of Zinc Coating on Zinc Coated Iron and Steel Articles

Scope: 1.1 This standard covers the procedure for determination of mass of coating zinc coated sheet, wire and other iron and steel articles.

Literature Survey Report

What is Zinc Plating?

Zinc plating is a process in which a thin layer of zinc is applied to the surface of a metal part. This is typically done through electroplating, where the metal part is submerged in a zinc-containing solution and an electric current is passed through, causing zinc to adhere to the part's surface.

The primary purpose of zinc plating is to provide corrosion resistance. Zinc acts as a sacrificial coating, corroding before the underlying metal does, thereby protecting it from rust and other forms of degradation.

Zinc plating is commonly known as galvanization or zinc electroplating. Both terms refer to the process of applying zinc as a protective barrier, though “galvanization” is often associated with a specific type, known as hot-dip galvanizing, which involves dipping the metal into molten zinc. Zinc electroplating, on the other hand, typically involves an electrolyte solution and electrical current to deposit the zinc layer.

Types of Zinc Plating

  - Yellow zinc plating: Yellow zinc plating involves applying a yellow chromate conversion layer over zinc, providing strong corrosion protection and a distinct golden appearance. Widely used in the automotive industry for fasteners, brake components, and brackets, it enhances durability against moisture and wear. While effective in extending part lifespan by reducing oxidation, its use of hexavalent chromate raises environmental concerns, limiting its eco-compatibility.

  - Clear or blue zinc plating: Clear or blue zinc plating provides a durable, environmentally friendly coating using trivalent chromates, avoiding harmful hexavalent compounds. Commonly used in automotive and electronics for fasteners and brackets, it offers moderate corrosion resistance with a clean finish. While safer and visually appealing, it provides less protection than yellow or black zinc plating in harsh environments.

  - Black zinc plating: Black zinc plating involves a black chromate coating over zinc, creating a matte, dark finish used in automotive and construction for screws, bolts, and brackets. It offers good corrosion resistance, reduces glare, and adds aesthetic value. However, the matte surface can be prone to scratches, making it slightly less durable in high-wear environments despite its visual and functional benefits.

  - Alkaline non-cyanide zinc plating: Alkaline non-cyanide zinc plating is a safer, eco-friendly process that eliminates hazardous cyanide from the plating bath. It offers good corrosion resistance and produces a smooth, uniform coating. Compatible with metals like steel and iron, it is ideal for industrial applications where environmental safety, reduced toxic waste, and reliable protective finishes are important priorities.

  - Zinc-nickel plating: Zinc-nickel plating, containing 10–15% nickel, offers superior corrosion resistance and durability, especially in harsh or coastal environments. Widely used in automotive and aerospace industries for components like engine parts and brake systems, it outperforms traditional zinc plating. Though effective against rust and salt spray, it requires precise control to ensure uniform alloy distribution during application.

  - Zinc-iron plating: Zinc-iron plating enhances corrosion resistance and wear strength by incorporating a small amount of iron into the zinc layer. Commonly used for fasteners, screws, and brackets in construction and industrial applications, it provides a durable, uniform coating. This method is ideal for components exposed to frequent handling or mechanical stress, offering improved rust protection over standard zinc plating.

  - Zinc-cobalt plating: Zinc-cobalt plating enhances hardness and corrosion resistance by alloying cobalt with zinc, making it ideal for high-wear applications. Commonly used in the automotive industry for trim and decorative parts, it offers a smooth, aesthetic finish with excellent durability. The cobalt improves adhesion and reduces chipping, ensuring long-term protection and reliability in demanding environments.

  - Acid zinc plating: Acid zinc plating uses an acidic electrolyte for faster deposition and better coverage on complex or recessed parts. Ideal for high-volume manufacturing, it provides a smooth, uniform finish. However, careful process control is needed to prevent over-plating and hydrogen embrittlement, which can compromise the metal’s structural integrity.

  - Boric acid zinc plating: Boric acid zinc plating is a specialized process that uses boric acid in the electrolyte to enhance coating smoothness and adhesion. It is ideal for electronics and small mechanical parts, offering excellent coverage in recessed or intricate areas. This method ensures uniform thickness and corrosion resistance, making it suitable for precision applications requiring consistent, stable finishes.

Main Parameters of Zinc Plating

- Thickness of Coating: The thickness of the zinc coating determines the level of protection provided. Thicker coatings generally offer better corrosion resistance, especially for parts exposed to harsh environments.

- pH Level: Maintaining the correct pH level in the plating solution is essential for consistent plating quality. The pH affects how smoothly the zinc ions deposit onto the part’s surface and can influence adhesion.

- Temperature: The temperature of the plating bath plays a significant role in the plating process. Higher temperatures generally increase the deposition rate but must be carefully controlled to prevent overheating, which could cause defects.

- Current Density: Current density impacts how quickly zinc ions deposit onto the metal surface. A consistent current density is crucial for achieving a uniform zinc layer, as fluctuations can lead to uneven coating thickness.

- Voltage: Voltage is applied across the plating bath to facilitate the transfer of zinc ions from the anode to the cathode. Correct voltage levels ensure efficient plating without causing excessive wear on the equipment or parts.

- Plating Time: The duration of time a part is submerged in the plating bath determines the thickness of the zinc layer. Longer times generally result in thicker coatings, though over-plating can lead to brittleness or poor adhesion.

Different Grades of Zinc Plating

The grading of zinc plating is based on thickness, impacting its durability and suitability for different environments. Here are the main grades:

- Fe/Zn 5: Minimum thickness of 5 microns, typically used for indoor parts with minimal exposure to moisture or harsh environments.

- Fe/Zn 8: Minimum thickness of 8 microns, suitable for parts needing moderate corrosion resistance, such as fasteners and hardware.

- Fe/Zn 12: Minimum thickness of 12 microns, ideal for components exposed to more demanding environments, like automotive parts or outdoor equipment.

How Zinc Plating Works:
Zinc plating uses electric current to deposit zinc ions onto a metal surface from an electrolyte solution. After cleaning the base metal, it is submerged in a zinc salt bath. A direct current drives zinc from the anode to the metal cathode, forming a protective, uniform zinc layer that resists corrosion. Post-plating treatments like chromate coatings may be applied to boost durability and adhesion.

Electrochemical Reactions:
At the anode, zinc oxidizes:
Zn (s) → Zn²⁺ + 2e⁻
Zinc ions migrate to the cathode, where they reduce and deposit:
Zn²⁺ + 2e⁻ → Zn (s)
This creates a solid zinc layer that acts as a sacrificial barrier, protecting the base metal from rust.

Steps of the Zinc Plating Process

  - Surface Cleaning:
Zinc plating starts with cleaning the metal to remove oil, dirt, and rust using alkaline cleaners or acids. This step is vital, as any surface contamination can prevent proper zinc adhesion during electroplating.

  - Preparing the Plating Solution:
The electrolyte bath is prepared with zinc salts like zinc sulphate or zinc chloride, along with additives to facilitate ion flow. A stable zinc ion concentration is crucial for uniform metal deposition.

  - Electroplating:
In this step, an electric current drives zinc ions from the anode to the metal cathode submerged in the solution. These ions deposit as a thin, even zinc layer, offering corrosion protection.

  - Rinsing and Drying:
After plating, the component is rinsed to remove solution residues and then dried. This prevents chemical deposits that could compromise the coating's integrity.

  - Post-Treatment:
A final passivation or sealing step is applied to enhance corrosion resistance. Chromate coatings are often used to extend durability and provide specific finishes like clear or yellow.

Post-Processing Activities in Zinc Plating

Post-processing is a critical phase in the zinc plating process, aimed at enhancing the corrosion resistance, durability, and overall performance of the coated component. These finishing treatments significantly extend the service life of the zinc layer and improve its aesthetic and functional properties.

The most widely used post-treatment is chromate conversion coating, which forms a passive barrier over the zinc surface. Available in finishes such as clear, yellow, or black, chromates not only increase corrosion resistance but also offer varied levels of visual appeal and protection, depending on application requirements.

Additionally, sealers are often applied as a topcoat to further reinforce the protective barrier. These sealers help prevent moisture ingress, improve surface smoothness, and enhance resistance to wear and abrasion.

Together, these post-processing activities ensure that zinc-plated components meet both environmental and operational demands across industries.

Chemicals Are Used for Zinc Plating: Several specific chemicals are used in the zinc plating process, particularly in the electrolyte solution and during surface preparation. These chemicals facilitate the electroplating reactions and ensure the zinc coating adheres correctly and provides the desired corrosion protection.

- Zinc Sulphate and Zinc Chloride: These are the primary sources of zinc ions in the plating bath. Zinc Sulphate is typically used in rack plating for its ability to produce bright, smooth finishes, while zinc chloride is preferred for barrel plating due to its efficiency in coating smaller or bulkier parts. The choice depends on the plating technique and part geometry.

- Additives: Electrolyte solutions are often enhanced with additives that improve deposit characteristics. Brighteners, levelers, and grain refiners are commonly used to achieve a smoother, glossier, and more uniform coating. These additives also contribute to improved current distribution and better surface coverage on complex parts.

- Acid or Alkaline Cleaners: Effective surface preparation is crucial for successful zinc plating. Alkaline cleaners remove grease and organic residues, while acidic solutions may be used for oxide or rust removal. Clean surfaces ensure strong adhesion and consistent zinc deposition, directly affecting the coating’s durability and appearance.

NOTE: The HSN codes for the chemicals used in the process could not be obtained, as the relevant data was not readily available from standard databases or official trade resources.

How Thick Should Zinc Plating Be

The thickness of zinc plating typically falls between 5 to 25 microns, depending on the level of corrosion protection required. Thicker coatings are used for parts exposed to harsh environments, while thinner coatings are suitable for indoor applications where there is minimal moisture exposure.

Specific thickness requirements vary by industry standards and depend on factors such as part function, expected wear, and exposure to corrosive elements. In automotive manufacturing, for example, thicker zinc layers are favoured for components that need extended durability and rust resistance.

How to Check Zinc Plating Thickness

There are a few reliable methods to measure the thickness of a zinc layer. The most common is x-ray fluorescence, a non-destructive method that measures coating thickness accurately by analysing the fluorescent x-rays emitted from the zinc coating.

Another approach is using a micrometre, a precision tool that can measure physical changes in thickness. Although slightly less precise, micrometres offer a practical and budget-friendly solution for quick checks. Each method ensures the coating meets required specifications for durability and protection.

What pH Level is Needed for Zinc Plating

The pH level of the plating solution is a critical factor in achieving a uniform zinc coating. For acid zinc plating, the optimal pH is generally between 4.8 and 5.5, whereas alkaline non-cyanide zinc baths typically maintain a pH around 11 to 13.

Controlling pH within these ranges helps ensure even zinc ion distribution across the plated surface and supports good adhesion. An imbalance in pH could lead to uneven coating, poor adhesion, or even failed electroplating, making precise pH monitoring essential in manufacturing processes.

What Temperature Is Zinc Plating Done

The typical temperature range for zinc plating is between 68°F and 86°F (20°C to 30°C). For certain applications, however, slightly elevated temperatures are used to accelerate the zinc deposition rate.

Too high a temperature can led to rapid zinc ion depletion in the plating solution, potentially reducing coating quality.

On the other hand, lower temperatures slow down the plating process and may compromise uniformity, so finding a balance within this range is important for achieving optimal results in both appearance and durability.

The maximum temperature for zinc plating generally hovers around 86°F to 95°F (30°C to 35°C). Higher temperatures can speed up the plating process but may lead to uneven deposition or compromised zinc quality. Staying within these limits ensures consistent adhesion and a uniform layer on the substrate, keeping the plating process efficient and effective.

Supported Materials for Zinc Plating

Zinc plating is versatile, providing effective corrosion resistance and a protective barrier for various base metals. Here are some commonly plated materials:

- Steel: The most commonly plated metal, steel benefits greatly from zinc plating’s corrosion protection. Zinc prevents rust on steel parts, extending their lifespan and making them suitable for applications in harsh conditions.

- Iron: Similar to steel, iron gains resistance to corrosion with zinc coating. Iron components plated with zinc are often used in outdoor and industrial settings where protection from rust is essential.

- Brass: Used in situations requiring good electrical conductivity, brass components benefit from zinc’s ability to protect against oxidation. Brass plating with zinc can also enhance appearance for applications where aesthetics matter.

- Copper: Frequently used in electronic and decorative applications, copper’s conductivity and finish can be further enhanced with a zinc layer. Zinc plating provides an added layer of oxidation resistance without affecting copper’s conductive properties.

Applications of Zinc Plating

Zinc plating has diverse applications across multiple industries, adding value to a wide range of components

- Automotive Parts: Zinc-plated bolts, nuts, and brake callipers benefit from extended durability and corrosion protection, making them suitable for vehicle applications where parts encounter moisture and varying temperatures.

- Hardware: Fasteners, brackets, and other hardware components often use zinc plating to resist rust, keeping them functional and durable over long periods.

- Military Equipment: Weapon systems and other military equipment benefit from zinc plating to withstand demanding environments while maintaining structural integrity.

- Electronics: Zinc plating is used on connectors and terminals to enhance conductivity while protecting the metal from rust, ensuring long-lasting performance in electronic devices.

- Construction: Structural components, metal frameworks, and other building materials are plated with zinc to enhance durability.

Benefits of Zinc Plating

Zinc plating provides an array of benefits, making it a popular choice across industries for coating metals:

- Corrosion Resistance: Zinc plating creates a barrier that protects the base metal from corrosion, adding years to the lifespan of steel, iron, and other materials.

- Enhanced Durability: This coating shields metals from wear and environmental factors, making plated parts more durable in challenging conditions.

- Improved Aesthetics: Zinc plating offers a clean and polished look. Finishes can range from bright to matte, which helps improve the visual appeal of hardware and industrial parts.

- Cost-Effectiveness: Zinc plating is more economical than other coatings, providing effective protection at a lower cost for high-volume manufacturing.

- Environmental Friendliness: Certain methods of zinc plating, such as alkaline non-cyanide zinc plating, are eco-friendly alternatives to cadmium, reducing harmful emissions.

- Electrical Conductivity: Zinc’s conductivity makes it suitable for electronic applications where corrosion protection and connectivity are both essential.

Limitations of Zinc Plating

- Limited Protection in Harsh Environments: In very aggressive environments, such as high salinity or extreme industrial exposure, zinc plating might not hold up as well as thicker coatings or specialized materials.

- Hydrogen Embrittlement: When plating high-strength steel, hydrogen embrittlement can occur, causing the metal to become brittle and reducing its load-bearing capacity if not properly treated.

- Reduced Effectiveness in Marine Environments: Zinc plating may struggle to withstand the high moisture and salt content typical of marine environments, often requiring additional coating layers.

- Thickness Variability on Complex Shapes: For parts with intricate designs or tight corners, achieving a uniform zinc layer can be challenging, potentially resulting in thinner spots susceptible to corrosion.

Factors to Evaluate the Quality and Durability of Zinc Plating

Evaluating the quality of a zinc-plated finish involves examining the consistency of the coating and its adherence to the base metal. Various factors impact the overall quality:

- Surface Preparation: Proper surface cleaning, often with a detergent solution, removes contaminants, ensuring that the zinc adheres fully to the metal surface, which is vital for a durable finish.

- Plating Bath Composition: The electrolyte solution used in the plating bath, with zinc ions and additional chemicals, plays a crucial role in achieving a uniform coating. The specific formulation influences coating thickness and smoothness.

- Current Density: In the electrodeposition process, the electrical current density affects the speed and thickness of the zinc layer. Careful adjustment is essential to avoid uneven or overly thick plating.

- Temperature Control: Operating the plating bath at optimal temperatures enhances zinc’s adherence and consistency. Temperature affects ion mobility and plating efficiency, with most processes maintained between 86°F to 95°F.

- Plating Time: Time is another critical factor, as longer plating duration allows for a thicker zinc layer. Balancing plating time ensures sufficient protection without unnecessary thickness that could lead to increased costs.

Test for Zinc Plating

Testing zinc plating involves evaluating both its durability and corrosion resistance. Common methods include salt spray testing and adhesion tests. Salt spray testing exposes the zinc-plated item to a saline mist, simulating corrosive conditions to measure how long the coating can resist rust. This test is a standard in many industries due to its effectiveness in assessing corrosion protection. Adhesion tests, on the other hand, check if the zinc layer properly bonds to the base metal.

NOTE: How Long Does Zinc Plating Last

Zinc plating can last up to 30 years under optimal conditions. However, its lifespan can vary depending on the environment it is exposed to. In dry, indoor conditions, the plating tends to endure longer, while outdoor and humid settings may reduce its longevity. For example, components used in coastal or marine environments may require additional protective layers to withstand constant exposure to saltwater and moisture, factors that accelerate corrosion.

Factors which depend on time taken for Zinc Plating

The zinc plating process generally takes several hours, but the exact time frame depends on a few factors:

- Size of the Part: Larger parts require more time to coat thoroughly due to their increased surface area, which may involve longer immersion times in the plating solution.

- Desired Coating Thickness: The thickness of the zinc layer directly affects processing time. Thicker coatings offer greater corrosion protection but take longer to deposit onto the metal surface.

- Type of Plating Method Used: Methods like barrel plating are often used for smaller parts and can be completed faster, while rack plating is more suitable for larger parts but takes more time due to careful placement and monitoring.

Common Problems and Defects with Zinc Plating

Zinc plating, while effective, can present several common issues:

- Blistering: Often resulting from inadequate cleaning, blistering can occur when contaminants remain on the metal’s surface before plating. To prevent this, you can ensure thorough pre-treatment and surface cleaning to remove oils, rust, and residues.

- Peeling: Peeling happens when the zinc layer doesn’t adhere properly, usually due to poor surface preparation. To address this, maintain correct plating bath pH and temperature levels, which support proper zinc ion bonding.

- Uneven Coating: Uneven coating may result from inconsistent current density or improper bath composition. Adjusting the plating bath chemistry and using precise current settings can produce a uniform zinc layer across all parts.

- Hydrogen Embrittlement: This issue arises when hydrogen gas, produced during plating, gets trapped in the metal, making it brittle. A post-plating baking process can help release trapped hydrogen, improving the durability and flexibility of the plated part.

Role of Zinc Plating in Environmental Sustainability

Zinc plating contributes to sustainability through its recyclable nature and eco-friendly practices in manufacturing processes. Unlike many coatings, zinc can be recycled, supporting a circular approach to metal use. Additionally, many zinc plating methods now emphasize reducing environmental impact by minimizing chemical waste and opting for less harmful electrolyte solutions, providing both durability and environmental benefits.

Different International Standards based on Zinc Electroplating:

  - ISO 2081: 2018(E) [Metallic and other inorganic coatings — Electroplated coatings of zinc with supplementary treatments on iron or steel]

Scope: This document specifies requirements for electroplated coatings of zinc with supplementary treatments on iron or steel. It includes information to be supplied by the purchaser to the electroplater, and the requirements for heat treatment before and after electroplating.

It is not applicable to zinc coatings applied

— to sheet, strip or wire in the non-fabricated form,

— to close-coiled springs, or

— for purposes other than protective or decorative.

This document does not specify requirements for the surface condition of the basis metal prior to electroplating with zinc. However, defects in the surface of the basis metal can adversely affect the appearance and performance of the coating.

The coating thickness that can be applied to threaded components can be limited by dimensional requirements, including class or fit.

  - ISO 1460: 2020(E) [Metallic coatings — Hot dip galvanized coatings on ferrous materials — Gravimetric determination of the mass per unit area]

Scope: This document specifies a method of determining the mass per unit area of hot dip galvanized coating on ferrous materials.

Since an exact knowledge of the area of the surface is essential, this document is mainly applicable to shapes whose areas are easy to determine. If, with heavy samples, the specifications cannot be met, then the hot dip galvanized coating mass is determined by another method.

  - ISO 10111: 2019 (E) [Metallic and other inorganic coatings — Measurement of mass per unit area — Review of gravimetric and chemical analysis methods]

Scope: This document gives guidelines for determining the average surface density over a measured area of anodic oxide or of a coating deposited autocatalytically, mechanically, by chemical conversion, by electrodeposition, by hot dip galvanizing and by chemical or physical vapour deposition using gravimetric and other chemical analysis procedures that have attained some degree of national or international standardization.

A variety of procedures are described and include:

— gravimetric procedures for chemical or electrochemical dissolution of the coating or the substrate to determine the coating surface density;

— gravimetric procedures for weighing the uncoated substrate and the coated (finished) specimen to determine the coating surface density;

— analytical procedures that utilize dissolution of the coating for determination of the coating surface density by instrumental chemical analysis methods.

With the exception of the gravimetric method as described in ISO 3892, this document does not give the measurement uncertainties of the methods cited.

Comparative study of Indian Standard [IS 1573] with International Standard [ISO 2081] based on Electroplated coatings of Zinc:

| Parameters present in IS 1573 | Corresponding parameters present in ISO 2081 | Remarks |
| --- | --- | --- |
| Specification for Electroplated Coatings of Zinc on Iron and Steel | Metallic and other inorganic coatings — Electroplated coatings of zinc with supplementary treatments on iron or steel |  |
| [Clause No. 1] Scope: [Clause No. 1.1] This standard covers requirement for electrodeposited zinc coatings applied to iron or steel articles except for coatings applied to components having threads of basic major diameter from 1.25 to 12.5 mm and coatings applied to sheet or wire in the unfabricated form or to close-coiled springs. [[Clause No. 1.2] Requirements are specified for appearance, thickness, adhesion, heat treatment before or after plating, precleaning standards, and if the coating is chromate- passivated, the corrosion resistance. | [Clause No. 1] Scope: This document specifies requirements for electroplated coatings of zinc with supplementary treatments on iron or steel. It includes information to be supplied by the purchaser to the electroplater, and the requirements for heat treatment before and after electroplating. It is not applicable to zinc coatings applied — to sheet, strip or wire in the non-fabricated form, — to close-coiled springs, or — for purposes other than protective or decorative. This document does not specify requirements for the surface condition of the basis metal prior to electroplating with zinc. However, defects in the surface of the basis metal can adversely affect the appearance and performance of the coating. The coating thickness that can be applied to threaded components can be limited by dimensional requirements, including class or fit. | The scope parameter is more detailed in ISO 2081, clearly specifying exclusions and including guidance on purchaser-supplier communication and application limits. |
| [Clause No. 2] Terminology: Surface, Significant Surface, Non-significant surface, Minimum local thickness, Minimum average thickness, Iridescent Passivation, Post-Plating Treatment, Hydrogen Embrittlement | [Clause No. 3] Terms, definitions, abbreviated terms and symbols | ISO 2081 includes a broader and more updated set of terms and definitions, incorporating modern electroplating language, whereas IS 1573 uses more traditional terms. Still, the key terminology concepts are equivalent. |
| [Clause No. 3] Coating Classification Number: [Clause No. 3.1] Manner of specifying requirements [Clause No. 3.2] grading of service conditions [Clause No. 3.3] classification of coating | Under [Clause No. 5] Designation- [Clause No. 5.1] General [Clause No. 5.2] Designation specification [Clause No. 5.3] Designation of the basis material | ISO 2081 combines designation details and classification within a single clause along with examples improving clarity for specification and procurement. Whereas IS elaborates the classification manner and grading. |
| [Clause No.4] Coating Requirements: [Clause No. 4.1] Finish and Appearance [Clause No. 4.1.2] Supplementary Treatments [Clause No. 4.2] Thickness and Type of Coating [Clause No. 4.4] Lustre [Clause No. 4.5] Corrosion Resistance [Coloured Coatings and Colourless Coatings] | Under [Clause No. 6] Requirements- [Clause No. 6.1] Appearance [Clause No. 6.2] Thickness [Clause No. 6.3] Trivalent chromium conversion coatings and other supplementary treatments [Clause No. 6.4] Adhesion of zinc and trivalent chromium conversion coatings [Clause No. 6.5] Accelerated corrosion testing | ISO 2081 organizes all coating-related parameters—appearance, thickness, corrosion resistance, and adhesion—under one comprehensive clause, offering a streamlined structure. IS 1573 spreads these across several clauses. Content-wise, both are equivalent.. |
| [Clause No.5] Basis Metal: [Clause No. 5.1] cleaning of Basis metal {high strength steels having a tensile strength greater than 1500MPa (corresponding hardness 440HV) should not be electroplated with zinc by conventional methods} | [Clause No. 5.3] Designation of the basis materials | Both standards highlight the importance of basis metal quality. IS 1573 specifically warns against plating high-strength steels over 1500 MPa using conventional methods, giving more prescriptive control, whereas ISO 2081 consolidates this within designation clauses |
| [Clause No.6] Heat Treatment: [Clause No. 6.1] performed to reduce the risk of damage by hydrogen embrittlement {Table for Categories of steels and maximum tensile strength corresponding to specified minimum tensile strength} [Clause No. 6.3] Stress Relief Before Plating {Table for Guidance of heat treatment for stress- relief before electroplating} [Clause No. 6.4] Heat treatment after Plating Hydrogen Embrittlement Relief {Table for Guidance of heat treatment for stress- relief after electroplating} [Clause No. 6.5] Activation Treatment. | [Clause No. 5.4] Designation of heat treatment requirements [Clause No. 6.6] Stress relief heat treatments before cleaning and metal deposition [Clause No. 6.7] Hydrogen- embrittlement- relief heat treatments after electroplating | ISO 2081 provides in-depth guidance on the heat treatment of surface-hardened steels to mitigate risks such as hydrogen embrittlement. In contrast, IS 1573 only states that conventional zinc electroplating should not be applied to hardened steels, without offering any technical direction or remedial process. |
| [Clause No. 7] Selection of Samples: [Clause No. 7.1] Out of each lot of similar parts, a number of samples shall be selected at random. The size of the lot and the number of samples to be selected shall be agreed upon between the manufacturer and the purchaser. All the samples selected shall be visually examined for any defects referred to in. | [Clause No. 7] Sampling | IS 1573 provides broader clarity and industry usability by detailing not only the method of random sampling and agreement between purchaser and manufacturer but also including clauses on rejection, packaging, and marking. This comprehensive approach makes IS 1573 more suitable for practical implementation in domestic manufacturing and inspection environments, ensuring a full cycle from sampling to final dispatch compliance. |
| [Clause No. 8] Test Specimens: [Clause No. 8.1] If separate test specimens are used to represent the coated articles in a test, the specimens shall be of same nature, size, and number and to be processed as required in the purchaser’s order. [Clause No. 8.2] Thickness and Adhesion Test specimens [Clause No. 8.3] Corrosion Resistance Test specimens [Clause No. 8.4] Hydrogen Embrittlement Test specimens. | Under [Clause No. 6] Requirements- [Clause No. 6.1] Appearance [Clause No. 6.2] Thickness [Clause No. 6.3] Trivalent chromium conversion coatings and other supplementary treatments [Clause No. 6.4] Adhesion of zinc and trivalent chromium conversion coatings [Clause No. 6.5] Accelerated corrosion testing [Clause No. 6.5.1] Neutral Salt Spray Test [Clause No. 6.5.2] Corrosion rating [Clause No. 6.6] Stress Relief Heat Treatment before cleaning and metal deposition. [Clause No. 6.7] Hydrogen-Embrittlement-Relief Heat Treatments after Electroplating | IS 1573 offers a more segmented view of test specimen usage, including criteria for different tests (adhesion, corrosion resistance, hydrogen embrittlement). ISO 2081 also provides specimen requirements but integrates them within general testing clauses. Moreover IS 1573 provides greater clarity by specifying how size and sample number should be mutually agreed upon. |
| [Clause No. 9] Test Methods: [Clause No. 9.1] Supplementary Treatments [Clause No. 9.2] Thickness [Clause No. 9.3] Adhesion [Clause No. 9.4] Corrosion Resistance [Clause No. 9.5] Visual Examination | Under [Clause No. 6] Requirements- [Clause No. 6.1] Appearance [Clause No. 6.2] Thickness [Clause No. 6.3] Trivalent chromium conversion coatings and other supplementary treatments [Clause No. 6.4] Adhesion of zinc and trivalent chromium conversion coatings [Clause No. 6.5] Accelerated corrosion testing [Clause No. 6.5.1] Neutral Salt Spray Test [Clause No. 6.5.2] Corrosion rating [Clause No. 6.6] Stress Relief Heat Treatment before cleaning and metal deposition. [Clause No. 6.7] Hydrogen-Embrittlement-Relief Heat Treatments after Electroplating [Annex A] Designation of Supplementary Treatments [Annex B] Measurement of average thickness of coating on small articles | IS 1573 distinctly lists test methods clause-wise, helping inspectors and manufacturers reference exact procedures. ISO 2081 consolidates them under broader headings. |

Comparative study of Indian Standard [IS 6745] with International Standard [ISO 1460 & ISO 10111] based on Electroplated coatings of Zinc:

| Parameter | IS 6745 Methods for Determination of Mass of Zinc Coating on Zinc Coated Iron and Steel Articles | ISO 1460 Metallic coatings — Hot dip galvanized coatings on ferrous materials — Gravimetric determination of the mass per unit area | ISO 10111 Metallic and other inorganic coatings — Measurement of mass per unit area — Review of gravimetric and chemical analysis methods | Remarks |
| --- | --- | --- | --- | --- |
| Scope & Applicability | Covers mass determination of zinc coating on iron/steel articles via stripping, volumetric, or gravimetric method | Specifies gravimetric method for hot-dip galvanized coatings where surface area is defined | Gravimetric for various metallic coatings on ferrous/non-ferrous substrates. | Both are equivalent in intent, though ISO 1460 is limited to hot-dip coatings and defined geometries; IS 6745 is broader zinc coating application. ISO 10111 extends applicability beyond ferrous materials. IS 6745 is broad; ISO 1460 is specific; ISO 10111 is flexible across coating types |
| Preparation Of test specimens from sample | Dimensions are mentioned separately for Galvanized Sheet, wire, tube. [Under Clause 3] | Not mentioned | Generalised statements are given [Under Clause 6] | Both IS 6745 and ISO 10111 provide similar guidance on the preparation of test specimens. However, ISO 10111 standard includes a specific clause addressing the dissolution of the substrate while preserving the integrity of thin coatings. It highlights the use of pre-heat treatment (e.g., 120 °C for 3 hours) to prevent curling or disintegration of coatings like thin gold layers during substrate removal. This practical guidance is not addressed in the corresponding Indian Standard (IS), which may lead to difficulties in accurately isolating and analysing thin coatings without damage. |
| Method Used | Clause 5- Stripping method using chemical dissolution similar principle as of Gravimetric method. | Clause 7- Gravimetric method: Determines coating mass per unit area via gravimetric calculation for defined shapes | Clause 8-Determination of mass of coating by chemical analysis. For each coating-substrate-reagent combination, there may be several analytical methods, e.g. photometric or volumetric methods, atom absorption spectroscopy or inductively coupled plasma with optical emission or mass spectrometry. Clause 9- Gravimetric determination of mass of coating | ISO & IS both uses mass per unit area for all cases, but IS specify the calculation formulae for different materials separately (for sheet, wires, and other than sheet wires) |
| Volumetric Method | Clause 6 – (Wires below 5mm in nominal diameter) Includes a volumetric method for steel wire with dimensional constants | Not covered [Only Gravimetric method followed] | Not mentioned separately. Clause 8.1 For each coating-substrate-reagent combination, there may be several analytical methods, e.g. photometric or volumetric methods, atom absorption spectroscopy or inductively coupled plasma with optical emission or mass spectrometry. | IS 6745 explains the volumetric method, whereas ISO 10111 does not mention so. |
| Surface Area Specification | Area considerations are specified fir different test sample accordingly | Requires exact surface area measurement for accurate results | Requires exact surface area measurement. Clause 7 – Measurement of coated area | ISO provides metrological clarity; IS could benefit from similar specificity. |
| Test Specimen Types | Includes sheets, wires exclusively along with other. | Primarily supports shapes with measurable surfaces | Ferrous and non-ferrous coated specimens of known area | IS is more comprehensive in specifying test articles. ISO 10111 offers broad specimen applicability, enhancing versatility |
| Method Of Calculation of mass of coating | 1. Mass per unit area (ρA) of the Galvanized sheet [in grams per square metre] ρA = (m1- m2)/ A × 106 2. Mass per unit area (ρA) of the Galvanized Wires [in grams per square metre] ρA = [(m1- m2)/ m2] ×d×1965 3. Mass per unit area (ρA) of other than Sheets & Wires [in grams per square metre] ρA = [(m1- m2)/ m2] ×t×3930 where: m1 (in g) mass of sample before stripping m2 (in g) mass of sample after stripping A is the area of exposed surface of sample d is diameter of stripped test piece (in mm) t is thickness of stripped test piece (in mm) [Under Clause 5] | 1. Mass per unit area (ρA) of the hot dip galvanized coating [in grams per square metre] ρA = (m1- m2)/ A × 106 where: m1 (in g) mass of sample before stripping, m2 (in g) mass of sample after stripping, A is the area of exposed surface of sample. [Under Clause 8] | Similar formula with unit conversion for mass per unit area The surface density, ρA, in milligrams per square centimetre, ρA = m/A where m is mass of coating (in mg), A is area (in sq.cm) The thickness, d, in micrometres d = 10 × ρA / ρC where: ρA is the surface density (in mg/ sq.cm) ρC is the density of coating (in g/ cubic cm) [Under Clause 10] | Same principle followed as of Stripping and Gravimetric method Only IS specify the calculation formulae for different materials separately IS has detailed formulas; ISO standards use simplified universal approach. |
| Test Report Requirement. | Not specified | Clause 9 – Test Report: Specifies mandatory reporting of method, specimen description, results in g/m² or µm, and observations. | Not mentioned | ISO 1460 ensures standardization and traceability of test outcomes. Both ISO standards support traceable, documented test outcomes; should be adopted in IS. |
| Precision and Measurement Accuracy | Based on accurate mass loss via dissolution | Based on surface area accuracy and consistent weighing | High precision with unified gravimetric methodology {a single, reliable, and accurate weight-based method used to measure coating thickness or mass per unit area across different coating types} | ISO provides a more controlled and repeatable approach for uniform samples. |
| Summary | IS 6745 provides valuable flexibility (volumetric (wire method), stripping methods), but reporting standards | ISO 1460 enforces gravimetric mass-area reporting and test documentation for hot-dip galvanized samples | ISO 10111 introduces a universal gravimetric method usable for various metallic coatings across substrate types | Revision of IS 6745 Based on ISO 1460 and ISO 10111 |

Recommendation –

- Revision of IS 1573 by adoption of ISO 2081in toto.

After analysing the comparison between IS 1573 and ISO 2081, it is recommended to adopt ISO 2081 in toto.

Notably, ISO 2081 provides in-depth guidance on the heat treatment of surface-hardened steels to mitigate risks such as hydrogen embrittlement. In contrast, IS 1573 only states that conventional zinc electroplating should not be applied to hardened steels, without offering any technical direction or remedial process.

Additionally, for specifications related to zinc anodes, IS 2605: 2023 may be referred to which can be added as an extra clause which can be worded as follows:

“Zinc Anode: The requirements of zinc anodes used for zinc electroplating may be as per IS 2605: 2023”

- Revision of IS 6745 with adopting modified ISO 10111

It is proposed to revise IS 6745 by adopting a modified ISO 10111, incorporating the volumetric method currently present in IS but absent in ISO. Since both standards detail gravimetric methods and chemical analysis based on the same principle, merging them into a single document will provide comprehensive guidance and simplify reference for users, ensuring alignment with international practices while retaining relevant Indian methodologies.

Refer the given draft made with the recommendation made: Annex_2

REFERENCE

website:

- https://www.3erp.com/blog/zinc-plating/#:~:text=The%20main%20types%20of%20zinc,it%20suitable%20for%20distinct%20applications

- https://www.approvedsheetmetal.com/blog/choosing-the-right-zinc-plating

- https://kdmfab.com/zinc-plating/

- BIS website: https://www.bis.gov.in/

- BIS Standards Portal: https://standardsbis.bsbedge.com/

Industry Survey Report

Name Of the Industry: Deepak Fasteners Ltd.

Date Of Visit: 02.06.2025

International Certification Industry holds:

- ISO 9001: 2015

- IATF 16949

- IATF 14001: 2015

- OHSAS 18001: 2007

- CE certified BS EN 14399 & 15048

- ISO/IEC 17025: 2017

Purpose: Blackening During Heat Treatment of Fasteners

Companies like Deepak Fasteners Ltd perform in-house heat treatment of their high-strength fasteners. During quenching (typically in oil):

- A black oxide scale naturally forms on the fasteners.

- This is a thermal blackening, not a post-process chemical black oxide treatment.

Fasteners may undergo light cleaning or oiling after quenching to preserve the black finish.

Blackening During Heat Treatment of Fasteners

When fasteners like bolts, nuts, and screws are manufactured, they often undergo a series of heat treatment processes to improve their mechanical properties such as hardness, strength, and toughness. The common sequence includes:

- Annealing

- Quenching

- Tempering

Among these, blackening occurs specifically during the quenching phase, and here's how:

What Happens During Quenching?

- After heating the fasteners to a high temperature (often in a furnace or controlled atmosphere chamber), they are rapidly cooled (quenched) in a medium — typically oil, sometimes water or polymer-based solutions.

- This rapid cooling helps to trap a hard microstructure (like martensite) within the steel, improving strength and hardness.

Why Do Fasteners Turn Black After Quenching?

- The surface of the steel reacts with oxygen, carbon, or oil vapours in the furnace or during quenching.

- This reaction forms a thin oxide layer on the metal surface — primarily iron oxide (Fe3O4, also called magnetite).

- This oxide scale appears black or blue-black in colour — hence the name "blackened fasteners".

This is not the same as a deliberate black oxide coating process, but rather a natural by-product of heat treatment and quenching in certain environments (especially oil-based quenching).

Why is this Blackened Finish Useful?

- While it’s not a functional anti-corrosion coating, this black scale offers mild oxidation resistance.

- It also helps with:

  - Part identification

  - Surface uniformity

  - Reduced glare or reflection

- Often, an oil coating is applied after quenching to seal the black surface and give additional rust protection.

Purpose: Zinc Plating Process

Zinc plating at Deepak Fasteners Ltd. is a critical finishing process designed to enhance corrosion resistance, improve product aesthetics, and meet international surface coating standards (e.g., ISO 2081, IS 1573). The facility utilizes both acid zinc and alkaline zinc plating techniques based on end-use application and customer requirements.

Zinc Plating Process

1. Surface Preparation

Purpose: Ensure clean, oxide-free metal surfaces for better zinc adhesion.

Steps:

- Degreasing: Removal of oils and lubricants using alkaline cleaners.

- Water Rinse: Deionized water used to eliminate chemical residues.

- Pickling (Acid Dip): Mild hydrochloric acid dip to remove rust or mill scale.

- Activation Dip: Final acid activation to condition the surface before plating.

Note: Strict monitoring of bath concentration and pH is done to ensure consistent cleaning efficiency.

2. Zinc Electroplating (Main Process)

Method: Acid Zinc Plating
Electrolyte Composition: Zinc chloride-based bath with ammonium salts and proprietary brighteners.

Key Parameters:

- Bath Temperature: 20–30°C

- Current Density: 1.0–3.0 A/dm²

- Plating Time: 10–30 minutes (depending on coating thickness requirement)

- Thickness Achieved: 5–25 µm

Equipment Used: Fully automated barrel plating and rack plating lines depending on component geometry.

Special Feature: Real-time process monitoring via SCADA ensures uniform thickness and finish.

3. Post-Plating Treatment

Passivation:

- Trivalent chromate conversion coatings applied (clear, blue, yellow chromate) for enhanced corrosion protection and appearance.

- Complies with RoHS regulations (Hexavalent chromium-free).

Drying: Hot air-drying chambers with humidity control to prevent white rust formation.

Fig1. Pre-Treatment or cleaning line, which is the initial step before zinc plating

Fig 2. Zinc Plating Process

Fig 3. Post-Treatment Steps

4. Quality Control & Testing

All finished components undergo the following tests:

Coating Thickness Measurement: Magnetic induction and XRF (as per ISO 3497)
Adhesion Test: Tape test or bend test
Corrosion Resistance: Neutral Salt Spray Test (ASTM B117) – min 72 hrs white rust resistance
Visual Inspection: Uniform finish, free from burns, pits, or discoloration

5. Environmental & Waste Management

The company has an ETP (Effluent Treatment Plant) for neutralizing plating effluents. Spent acid and metal sludge are disposed of as per PCB norms. Zinc recovery systems help in minimizing wastage and recycling rinse waters.

Specification Chart: Provided by Industry

ANNEX 1

INTERNATIONAL                                                                 ISO

STANDARD                                                                        11408

Chemical Conversion Coatings – Black Oxide Coating on Iron and Steel – Specification and test methods

Contents                                                                                                                                              Page

- Scope.............................................................................................................................................1

- Normative references....................................................................................................................1

- Term and definition ......................................................................................................................2

- Information to be supplied by the purchaser to the supplier.........................................................2

4.1 Essential information...............................................................................................................2

  - Additional information ............................................................................................................2

- Substrate ......................................................................................................................................2

- Heat treatment of steels ...............................................................................................................3

6.1General......................................................................................................................................3

  - Heat treatment before black oxidizing.......................................................................................3

  - Heat treatment after black oxidizing .........................................................................................3

- Procedure

7.1 Surface Preparation………………………………………………………………………….3

7.2 Application of Black Coating………………………………………………………………..3

7.3 Rinsing……………………………………………………………………………………….3

7.4 Sealing……………………………………………………………………………………….3

- Requirements................................................................................................................................4

8.1 Appearance and surface quality ...............................................................................................4

8.2 Oxalic acid test resistance........................................................................................................4

8.3 Resistance of austenitic stainless steels to neutral salt spray...................................................4

8.4 Adhesion Test — Cross- Cut Test …………………………………………….…………..4

8.5 Coating Thickness Measurement……………………………………………………...…4

- Sampling........................................................................................................................................4

Annex A (informative) Processing procedures for iron and stainless steels.............................................6

Annex B (informative) Methods of test for neutral surface reaction and for porosity and continuity………………………………………………………………………………………................7

Foreword

ISO (the International Organization for Standardization) is a worldwide federation of national standards bodies (ISO member bodies). The work of preparing International Standards is normally carried out through ISO technical committees. Each member body interested in a subject for which a technical committee has been established has the right to be represented on that committee. International organizations, governmental and non-governmental, in liaison with ISO, also take part in the work. ISO collaborates closely with the International Electrotechnical Commission (IEC) on all matters of electrotechnical standardization.

International Standards are drafted in accordance with the rules given in the ISO/IEC Directives, Part 3.

Draft International Standards adopted by the technical committees are circulated to the member bodies for voting. Publication as an International Standard requires approval by at least 75 % of the member bodies casting a vote.

International Standard ISO 11408 was prepared by Technical Committee ISO/TC 107, Metallic and other inorganic coatings, subcommittee SC 8, Chemical conversion coatings.

Modifications are made under Clause no. 4.1 and 4.2 which are the important parameter to take care. Another modification done under Clause no. 6.2

A new clause titled “Procedure” has been incorporated in the standard. This clause includes sub-sections on Surface Preparation, Application of Black oxide coating, Rinsing and Sealing.

Under Clause no. 8, two more clauses based on test are being added, that are Adhesion Test and Coating Thickness Measurement.

Annexes A and B of this International Standard are for information only.

Chemical Conversion Coatings – Black Oxide Coating on Iron and Steel – Specification and test methods

1 Scope

This International Standard specifies requirements for black oxide coatings on iron and steel (including cast and wrought iron, carbon steel, low alloyed steel and stainless steel). Black oxide coatings can be used to diminish friction between sliding or bearing surfaces or for decorative purposes or to reduce light reflection. Such coatings, with or without supplementary preservative treatment, may be used where a black surface is required. Only very limited corrosion protection is obtained under mildly corrosive conditions even with preservative treatment.

This International Standard does not specify requirements for the condition, finish or surface roughness of the substrate prior to black oxidizing.

2 Normative references

The following normative documents contain provisions which, through reference in this text, constitute provisions of this International Standard. For dated references, subsequent amendments to, or revisions of, any of these publications do not apply. However, parties to agreements based on this International Standard are encouraged to investigate the possibility of applying the most recent editions of the normative documents listed below. For undated references, the latest edition of the normative document referred to applies. Members of ISO and IEC maintain registers of currently valid International Standards.

ISO 2064:1996, Metallic and other inorganic coatings — Definitions and conventions concerning the measurement of thickness.

ISO 2409: 2020(E), Paints and varnishes — Cross-cut test

ISO 4519, Metallic and other inorganic coatings — Sampling procedures for inspection by attributes.

ISO 9227, Corrosion tests in artificial atmospheres — Salt spray tests.

ISO 9587, Metallic and other inorganic coatings — Pre-treatments of iron and steel to reduce the risk of hydrogen embrittlement.

ISO 9588, Metallic and other inorganic coatings — Post coating treatments of iron and steel for reducing the risk of hydrogen embrittlement.

ISO 16809: 2017(E), Non-destructive testing — Ultrasonic Thickness Measurement.

3 Term and definition

For the purposes of this International Standard, the following term and definition apply.

3.1 significant surface: part of the article covered or to be covered by the coating and for which the coating is essential for serviceability and/or appearance and where the coating has to meet all of the specified requirements [ISO 2064:1996, definition 3.1]

4 Information to be supplied by the purchaser to the supplier

4.1 Essential information

When ordering articles to be black oxide coated in accordance with this International Standard, the purchaser shall provide the supplier with the following information:

- the number of this International Standard, i.e. ISO 11408;

- the significant surface of the article to be coated, indicated, for example, on a drawing or by the provision of suitably marked samples;

- the nature and surface condition (see clause 5) of the substrate;

- the sampling procedure to be adopted (see clause 8);

- the appearance of the coating, e.g. by the provision of a suitably marked sample (see 7.1).

- the base material or the specific grade of iron & steel of the article to be coated so that particular process can be carried out following Table A.1

4.2 Additional information

The following additional information may be provided by the purchaser as appropriate:

- whether the neutral surface reaction has to be tested (see B.1);

- whether porosity and continuity (gross defect) of the black oxide coating has to be tested (see B.2);

- any requirements for supplementary preservative treatment (e.g. oil, wax or lacquer films) and humidity testing after such treatment;

- any requirements for heat treatment before and/or after black oxidizing (see clause 6);

- any requirements for oxalic acid resistance testing (see 8.2);

- any requirements for wear resistance and its measurement;

- any requirements for coefficient of friction and its measurement;

- any requirements for resistance to neutral salt spray (see 8.3);

- any requirements for adhesion with thicker black oxide coatings. (see 8.4)

- any requirements for thickness measurement of the black oxide coating and the preferred method of measurement. (see 8.5)

5. Substrate

The surface roughness of the coating will be dependent on the initial roughness of the substrate and this shall therefore not be cause for rejection of the black oxide coating.

6 Heat treatment of steels

6.1 General

Heat treatment may be required for certain steel grades to reduce the risk of cracking by hydrogen embrittlement or caustic brittleness.

CAUTION — High strength steel, of tensile strength Rm > 1 000 MPa, may be subjected to caustic embrittlement that could lead to spontaneous cracking under internal or applied stress during the black oxidizing process.

6.2 Heat treatment before black oxidizing

Pre-treatment shall be carried out in accordance with ISO 9587. The heat treatment shall be carried out before the commencement of any preparation or cleaning treatment using aqueous solutions. The heat treatment may be performed at a temperature between 200 °C and 230 °C for not less than 2 h prior to any surface preparation or cleaning using aqueous solutions.

6.3 Heat treatment after black oxidizing

Post-coating treatment shall be carried out in accordance with ISO 9588. Surface-hardened parts shall be heat treated at a temperature between 190 °C and 220 °C for not less than 2 h.

7. Procedure

7.1 Surface Preparation

Prior to the application of the black coatings, the basis metal shall be thoroughly cleaned. The cleaned surfaces shall be free of rust, scale, grease, oil, paint, or other foreign matter. The cleaning process shall be performed without measurable abrasion or erosion unless specified or as agreed between supplier and purchaser.

7.2 Application of Black Coating

Unless otherwise specified, the black coatings shall be applied after all machining, forming, welding, cold straightening and heat treatment have been completed.

The process includes a chemical reaction wherein, upon immersion in the oxidizing solution, the iron on the surface of the metal reacts with oxidizing salts to form a layer of magnetite, resulting in the characteristic black oxide finish.

The specified black coating shall be applied under controlled procedural conditions, especially with respect to time and temperature, in accordance with Table A.1

7.3 Rinsing

Black oxide coated pieces shall be rinsed in ambient clean water. Non- chlorinated water should be avoided to prevent any corrosion attack.

7.4 Sealing

Black oxide coated pieces shall be immersed in oil, wax. The sealing shall be carried out immediately after rinsing to prevent oxidation.

8 Requirements

8.1 Appearance and surface quality

The coating shall be free of spots of red oxide and shall not be an overall reddish-brown colour. When a part is wiped with a clean Whatman 40 filter paper (or other filter paper of equivalent quality) prior to application of any supplementary preservative treatment, it shall produce no reddish-brown or green smut.

NOTE non-uniformity of colour and haze is permissible on parts that are locally hardened, welded, cemented, riveted or submitted to other kinds of mechanical treatment.

8.2 Oxalic acid test resistance

8.2.1 When tested in accordance with 7.2.2 prior to the application of any supplementary preservative treatment, the black oxide coating on a part shall conform to Figure 3.

8.2.2 Dissolve 50 g oxalic acid in 1 l of distilled or de-ionized water. Place three drops (; 0,2 ml) of the solution on a flat spot of the black oxide coated surface at ambient temperature. The reaction should occur after 30 s and within 8 min. After 8 min rinse and dry the surface and compare it to Figures 1 to 3.

8.3 Resistance of austenitic stainless steels to neutral salt spray

When tested using the salt spray test (NSS test) in accordance with ISO 9227, the significant surface, without any supplementary preservative coating, shall withstand 96 h without displaying traces of corrosion (rust).

8.4 Adhesion Test — Cross- cut Test

8.4.1 When tested in accordance with 8.4.2, the black oxide coating shall exhibit no significant flaking or detachment.
8.4.2 Apply a pressure-sensitive adhesive tape (as per ISO 2409) firmly onto the coated surface. Examine the tape and substrate for coating removal. The coating is considered to have passed if no coating detachment beyond minor edge flaking is observed.

8.5 Coating Thickness Measurement

8.5.1 When tested in accordance with 8.5.2, the thickness of the black oxide coating shall be measured to ensure compliance with specified dimensional limits, depending on the process used.

8.5.2 For non-destructive coating thickness measurement, the ultrasonic method shall be used in accordance with ISO 16809. This technique is suitable for coatings on both magnetic and non-magnetic substrates and operates on the pulse-echo principle, wherein an ultrasonic pulse is transmitted into the coated surface and the time taken for the echo from the coating-substrate interface is measured. The thickness is determined based on the time delay and the known acoustic velocity of the coating material. The probe shall be placed perpendicular to the coated surface, and readings shall be noted.

9 Sampling

A random sample of the size required by ISO 4519 shall be selected from the inspection lot. The articles in the sample shall be inspected for conformance to this International Standard and the lot shall be classified as conforming or not conforming to each requirement according to the criteria of the sampling plans in ISO 4519.

Figure 1 — Poor quality coating

Figure 2 — Borderline quality coating

Figure 3 — Good quality coating

Annex A

(informative)

Processing procedures for iron and stainless steels

- Subsequent tanks, if used, are made from the same chemicals at increased concentrations relative to the previous tank.

- Less than 8 % nickel

Table A.1 — Typical processing procedures for steels and stainless steels

| Iron and steel grades | Process and suitable chemicals | Processing Temperature °C | Immersion time min |
| --- | --- | --- | --- |
| Carbon steels, low alloy steels, wrought irons, cast irons | Alkaline oxidizing: NaOH, NaNO3, water | Processing tanka boiling at 130 to 150 | 15 to 60 |
| Martensitic stainless steel tempered at less than 480 °C | Alkaline-chromate: NaOH, NaNO3, Na2Cr2O7 | 115 to 125 | 30 to 45 |
| Martensitic stainless steel tempered at 480 °C or higher | Fused salt; oxidizing: Na2Cr2O7 and/or K2Cr2O7 | Molten salt bath 400 to 455 | 30 |
| Stainlessb steels (ferritic and austenitic) | Alkaline oxidizing |  |  |

Table A.2 — Different grades of stainless steels

| Stainless steel grades | Nickel content % | Hardenability |
| --- | --- | --- |
| Ferritic | - | Non-hardenable |
| Martensitic | < 2.5 | Hardenable |
| Ferritic-austenitic | 4.5 to 7 | Non-hardenable |
| Austenitic | 7 to 26 | Non-hardenable |

Annex B

(informative)

Methods of test for neutral surface reaction and for porosity and continuity

B.1 Neutral surface reaction

The test shall be carried out after the last rinsing and drying, but before the oiling. Phenolphthalein test solution or phenolphthalein indicator paper shall be used as follows.

- Prepare phenolphthalein test solution by dissolving 2 g of phenolphthalein in 100 ml of ethanol and keep the solution in a glass dropping bottle. Place 1 to 2 drops of the test solution on the surface to be tested (joints, cavities).

- Moisten the phenolphthalein indicator paper with distilled water and place this paper on the surface to be tested.

Residual alkalis shall be deemed to be present if the phenolphthalein drops or indicator paper (as appropriate) turn a rose colour.

B.2 Porosity and continuity of the black oxide coating

The test shall be conducted by immersion (a) or using droplets (b).

Ensure that each test uses a fresh test solution prepared from laboratory reagent grade CuSO4 at a mass fraction of 3 %.

- Immerse the specimen in the test solution (in a glass or plastic bottle) at a temperature of 15 °C to 20 °C. After 30 s remove the specimen, rinse it using cold water and dry it using filter paper.

- Place three drops of the test solution on the surface to be tested. After 30 s remove the drops using filter paper.

Examine the surface under normal corrected vision. Red points or spots shall be deemed to indicate the presence of pores or that the coating is damaged.

ANNEX 2

INTERNATIONAL                                                                 ISO

STANDARD                                                                         10111

Metallic and other inorganic coatings — Measurement of mass per unit area — Review of gravimetric and chemical analysis methods

Contents                                                                                                                                           Page No.

Foreword

- Scope..............................................................................................................................................1

- Normative references......................................................................................................................1

- Terms and definitions......................................................................................................................1

- Principle...........................................................................................................................................2

- Special equipment............................................................................................................................2

- Preparation of test specimen............................................................................................................2

6.1 Size.......................................................................................................................................... 2

6.2 Shape....................................................................................................................................... 2

6.3 Edge condition..........................................................................................................................2

6.4 Heat treatment..........................................................................................................................2

- Measurement of coated area...........................................................................................................3

7.1 Measurement method...............................................................................................................3

7.2 Surface measuring equipment..................................................................................................3

7.2.1 Geometrical (projected) surface area............................................................................3

7.2.2 Surface area increase due to roughness (optional).......................................................3

  - Number of measurements.................................................................................................3

- Determination of mass of coating by chemical analysis................................................................4

8.1 General......................................................................................................................................4

  - Restrictions...............................................................................................................................4

- Gravimetric determination of mass of coating.............................................................................4

9.1 Specimen size........................................................................................................................4

9.2 Limitations.............................................................................................................................4

9.3 Restrictions............................................................................................................................4

9.4 Gravimetric analysis equipment............................................................................................4

9.5 Procedure................................................................................................................................5

9.5.1 General..........................................................................................................................5

9.5.2 Difference method with dissolution of the coating........................................................5

9.5.3 Direct weighing method with dissolution of the substrate............................................5

    - Difference method without dissolution......................................................................5

- Calculation……………………………………………………………………………………….6

10.1 Surface Density…………………………………………………………………………..6

10.2 Thickness…………………………………………………………………………………6

- DETERMINATION OF MASS OF COATING ON WIRE

(BELOW 5 mm IN NOMINAL DIAMETER) BY VOLUMETRIC METHOD………………………………6

11.1 Outline of the Method……………………………………………………………………....6

11.2 Reagents………………………………………………………………………………….…6

11.3 Apparatus…………………………………………………………………………………..7

11.4 Preparation of Test Piece………………………………………………………………......7

11.5 Cleaning of Test Piece………………………………………………………………….…...7

11.6 Procedure……………………………………………………………………………………7

11.7 Calculation………………………………………………………………………………….8

Annex A (informative) Reagents for selective dissolution of metal layers...................................................9

Bibliography..................................................................................................................................................14

Foreword

ISO (the International Organization for Standardization) is a worldwide federation of national standards bodies (ISO member bodies). The work of preparing International Standards is normally carried out through ISO technical committees. Each member body interested in a subject for which a technical committee has been established has the right to be represented on that committee. International organizations, governmental and non-governmental, in liaison with ISO, also take part in the work. ISO collaborates closely with the International Electrotechnical Commission (IEC) on all matters of electrotechnical standardization.

The procedures used to develop this document and those intended for its further maintenance are described in the ISO/IEC Directives, Part 1. In particular, the different approval criteria needed for the different types of ISO documents should be noted. This document was drafted in accordance with the editorial rules of the ISO/IEC Directives, Part 2 (see www .iso .org/directives).

Attention is drawn to the possibility that some of the elements of this document may be the subject of patent rights. ISO shall not be held responsible for identifying any or all such patent rights. Details of any patent rights identified during the development of the document will be in the Introduction and/or on the ISO list of patent declarations received (see www .iso .org/patents).

Any trade name used in this document is information given for the convenience of users and does not constitute an endorsement.

For an explanation of the voluntary nature of standards, the meaning of ISO specific terms and expressions related to conformity assessment, as well as information about ISO's adherence to the World Trade Organization (WTO) principles in the Technical Barriers to Trade (TBT) see www .iso .org/iso/foreword .html.

This document was prepared by Technical Committee ISO/TC 107, Metallic and other inorganic coatings.

This second edition cancels and replaces the first edition (ISO 10111:2000), which has been technically revised. The following changes have been made:

a) a gravimetric method has been added for weighing the uncoated substrate and the finished sample;

b) the surface area increase caused by surface roughness has been considered to obtain a more realistic estimation of local geometric coating thickness (optional);

c) Annex A, which gives reagents for etching or stripping solutions, has been changed to informative as other solutions can be applied;

d) reagents in Annex A that referred to no longer existing standards or which contain hazardous chemicals have been removed;

e) outdated and uncited references in the Bibliography have been removed.

A new clause titled “Determination of mass of coating on wire (below 5mm in nominal diameter) by Volumetric Method” has been incorporated in the standard. This clause includes sub-sections on the reference standard (IS 2605), Outline of the method, Reagents, Preparation of test piece, Cleaning of test piece, Procedure, Calculation.

Any feedback or questions on this document should be directed to the user’s national standards body. A complete listing of these bodies can be found at www .iso .org/members .html.

Metallic and other inorganic coatings — Measurement of mass per unit area — Review of gravimetric and chemical analysis methods

WARNING — The use of this document can involve hazardous materials, operations and equipment. It does not purport to address all of the safety or environmental problems associated with its use. It is the responsibility of users of this document to take appropriate measures to ensure the safety and health of personnel and the environment prior to application of this document.

- Scope

This document gives guidelines for determining the average surface density over a measured area of anodic oxide or of a coating deposited autocatalytically, mechanically, by chemical conversion, by electrodeposition, by hot dip galvanizing and by chemical or physical vapour deposition using gravimetric and other chemical analysis procedures that have attained some degree of national or international standardization.

A variety of procedures are described and include:

— gravimetric procedures for chemical or electrochemical dissolution of the coating or the substrate to determine the coating surface density;

— gravimetric procedures for weighing the uncoated substrate and the coated (finished) specimen to determine the coating surface density;

— analytical procedures that utilize dissolution of the coating for determination of the coating surface density by instrumental chemical analysis methods.

With the exception of the gravimetric method as described in ISO 3892, this document does not give the measurement uncertainties of the methods cited.

- Normative references

The following documents are referred to in the text in such a way that some or all of their content constitutes requirements of this document. For dated references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies.

ISO 2080, Metallic and other inorganic coatings — Surface treatment, metallic and other inorganic coatings — Vocabulary

- Terms and definitions

For the purposes of this document, the terms and definitions given in ISO 2080 apply.

ISO and IEC maintain terminological databases for use in standardization at the following addresses:

— ISO Online browsing platform: available at https://www.iso.org/obp

— IEC Electropedia: available at http://www.electropedia.org/

- Principle

The mass of a coating over a measured area is determined by

a) weighing the test specimen before and after dissolving the coating in a reagent or electrolyte that does not attack the substrate, or

b) weighing the coating after dissolving the substrate in a reagent that does not attack the coating, or

c) dissolving both the coating and the substrate, or the coating alone, and quantitatively analysing the resulting solution, or

d) weighing the test specimen before and after the coating process, provided that the mass of the substrate material removed during those pre-treatment steps, after which a weighing would negatively affect the coating deposition steps, is negligible compared to the mass of the coating.

The surface density of the coating is calculated from the mass and area measurements. Its thickness is based on the mass, area and density of the coating material.

- Special equipment

Certain specialized chemical, electrochemical and chemical analysis equipment is required for some of the specific methods referred to in Table A.1 (see Clauses 8 and 9).

- Preparation of test specimen

  - Size

The specimen should be large enough to permit area and mass measurement of adequate accuracy (see Clauses 8 and 9).

  - Shape

The shape of the test specimen should be such that the surface area can be readily measured without difficulty. A rectangular or circular test specimen is usually suitable.

  - Edge condition

If the area to be measured is small and has to be known accurately, the edges may need to be dressed to remove smeared coating, to remove loose burrs and to provide well-defined and (for rectangles) straight edges. This should be considered for areas less than 100 mm2.

One method of dressing the edges of a rectangular specimen involves clamping the specimen between two plastic or metal blocks with the edge of the specimen flush with the edges of the blocks and then grinding and polishing the edges metallographically.

  - Heat Treatment

If the substrate has to be dissolved in such a way as to leave the coating intact, it may be desirable to first treat the test specimen so that the coating will not curl up tightly or fall apart. Some gold deposits of 1.5 mg/cm2 (< 0.9 μm) will fall apart when their substrates are dissolved, but will support themselves after heat treatment at 120 °C for 3 h. If the thickness of a coating (instead of its surface density) is being determined, a heat treatment that could change the density of the coating material should not be used.

- Measurement of coated area

7.1 Measurement method

Since the accuracy of the area measurement should be greater than the desired accuracy of the surface density measurement, the method of measuring the area depends on the desired accuracy and the specimen size.

7.2 Surface measuring equipment

7.2.1 Geometrical (projected) surface area

The area can be measured with a planimeter, but it is usually determined by linear measurements. Often a micrometre or vernier calliper is used. For large areas, however, a ruler may do.

For maximum accuracy, a measuring microscope should be used.

It may be difficult to measure directly the area of threaded articles with sufficient accuracy, in which case the area should be determined from drawings or published tables.

7.2.2 Surface area increase due to roughness (optional)

Surface roughness leads to an increase of the true surface area compared to the geometrical (projected) surface area as determined by the methods described in 7.2.1.

Using atomic force microscopy (AFM), confocal microscopy or interference microscopy and a suitable computer software, the relative surface area increase (RSAI) can be determined (at least for a small fraction of the total surface).

Enhance the geometrical (projected) surface by the RSAI to estimate the true surface area. Calculate the true surface density of the coating or the true coating thickness using this true surface area in order to obtain a better agreement with geometrical coating thickness measurements in cross-section.

The RSAI should be determined on the uncoated substrate before any coating is applied as some coatings tend to level surface roughness, but preferably after pre-treatment steps, which increase surface roughness, e.g. to improve adhesion.

7.3 Number of measurements

Because circular or rectangular specimens will not be perfectly circular or rectangular, each dimension should be measured in three places. For a rectangle, the length of each edge and the length and width through the centre should be measured and an average obtained for each dimension.

NOTE    In the case of a cylinder, one would normally measure the diameter and length. In specifications for metallic coated wire (fencing) that has been electroplated or coated by other processes, the length of the wire specimen is not measured, but is, in effect, calculated from the mass (which is measured anyway), the radius and the density of the substrate material as follows:

l = m / (π r3 ρs)

where l is the length

m is the mass

r is the radius

ρs  is the density of the substrate.

8 Determination of mass of coating by chemical analysis

8.1 General

The chemical analysis method is very general. Both coating and substrate or the coating alone are dissolved in a suitable reagent (see Annex A for examples) and then the resulting solution is analysed for the coating material. For each coating-substrate-reagent combination, there may be several analytical methods, e.g. photometric or volumetric methods, atom absorption spectroscopy or inductively coupled plasma with optical emission or mass spectrometry.

8.2 Restrictions

The chemical analysis method cannot be used when the coating material cannot be completely removed from the substrate material by chemical means or when there is a constituent common to both that is not readily separated (e.g. nickel phosphorus alloy on nickel).

9 Gravimetric determination of mass of coating

9.1 Specimen size

Since the measurement uncertainty of the mass measurement should be less than the desired measurement uncertainty of the surface density measurement, the test specimen should be large enough for the coating to be weighed with the desired accuracy (see 9.2).

9.2 Limitations

In principle, the gravimetric procedures can be used to measure very thin coatings or to measure coatings over small areas, but not thin coatings over small areas. The limits depend on the required accuracy, e.g. 2,5 mg/cm2 of coating might require 1 cm2, but 0,1 mg/cm2 of coating would require 25 cm2 to obtain 2,5 mg of coating.

The gravimetric method does not indicate the presence of bare spots or sites with thicknesses lower than the specified minimum in the measuring areas. In addition, the single value obtained from each measuring area is the mean thickness of that area.

The measurement uncertainty of the gravimetric method is normally less than 5 % over a wide range of thicknesses (see ISO 3892).

9.3 Restrictions

The gravimetric procedures can be used for many coating–substrate combinations. Except for the procedure described in 9.5.4, they cannot be used where neither the coating nor substrate material can be completely removed, one from the other by chemical or physical means.

9.4 Gravimetric analysis equipment

A balance is required for gravimetric analysis, but the required sensitivity of the balance depends on the size of the test specimen, the coating thickness (coating mass) and the required accuracy of the measurement. The analytical balance should be capable of weighing to an accuracy of 0,1 mg for weighing the test pieces under examination before and after dissolution of the coatings or before and after the coating process, respectively.

For anodic and cathodic dissolution, a (constant) direct current source is necessary.

9.5 Procedure

9.5.1 General

The mass of coating may be determined by

- weighing the test specimen before and after dissolving the coating (see Annex A for exemplary reagents) and taking the difference (see 9.5.2), or

- dissolving the substrate (see Annex A for exemplary reagents) and weighing the coating directly (see 9.5.3), or

- weighing the test specimen before and after deposition of the coating and taking the difference (see 9.5.4).

The first time a gravimetric method is used, it should be evaluated in accordance with 9.5.2.2 and 9.5.3.2.

9.5.2 Difference method with dissolution of the coating

9.5.2.1 First, clean the test specimen of any foreign material, then rinse it with alcohol (methanol, ethanol, isopropanol) or another suitable solvent, blow it dry with clean air and weigh it. Immerse the specimen in the appropriate reagent (see Annex A for examples) to dissolve the coating either chemically or electrochemically, rinse it with water, then with alcohol, blow it dry with clean air and weigh it again. The loss of mass is the mass of the coating.

9.5.2.2 To determine if any dissolution of the substrate has occurred, repeat the process with the stripped substrate, making sure that the substrate is immersed in the reagent for the same length of time as before. Any loss of mass enables one to make a judgement of a possible error due to any dissolution of the substrate with the coating during the stripping process.

9.5.3 Direct weighing method with dissolution of the substrate

9.5.3.1 Dissolve the substrate in the appropriate reagent (see Annex A for examples). Rinse the coating with water and then alcohol (methanol, ethanol, isopropanol) or another suitable solvent, blow it dry with clean air and weigh it.

9.5.3.2 To determine if any dissolution of the coating occurred, submit the isolated coating to the same stripping process, making sure that the coating is immersed in the stripping reagent for the same length of time as it was during the stripping process. Any loss of mass enables one to make a judgement of a possible error due to any dissolution of the coating with the substrate during the stripping process.

9.5.4 Difference method without dissolution

First, clean the uncoated test specimen of any foreign material, rinse it with alcohol or another suitable solvent, which does not attack the substrate material nor disturb the subsequent coating process, blow it dry with clean air and weigh it.

Then subject the uncoated test specimen to the coating process.

Afterwards, clean the coated test specimen of any foreign material, rinse it with alcohol or another suitable solvent, which attacks neither the coating nor uncovered zones of the substrate, blow it dry with clean air and weigh it.

The gain of mass is the mass of the coating.

As many of the required pre-treatment steps for the substrate material as possible should be done before the first weighing, especially when they remove substrate material. However, pre-treatment steps, which are integral part of the coating process and do not allow for an interruption for weighing, e.g. wet in wet or without breaking the vacuum, cannot be done before weighing. When such pre-treatment steps remove substrate mass, which is a significant fraction or even a multiple of the coating mass, the method described in this subclause cannot be applied.

- Calculations

10.1 Surface density

Calculate the surface density, ρA, in milligrams per square centimetre, from Formula (1):

ρA = m/A                                                                                                                                  (1)

where

m is the mass of coating, in milligrams;

A is the area, in square centimetres.

10.2 Thickness

Calculate the thickness, d, in micrometres, from Formula (2):

d =10 × ρA / ρC                                                                                                                               (2)

where

ρA   is the surface density, in milligrams per square centimetre;

ρC is the density of the coating in grams per cubic centimetre.

NOTE    The density of a coating metal is usually not the same as the published values of bulk or wrought metal. For example, the density of electrodeposited gold is generally less than 19.3 g/cm3 and sometimes as low or lower than 17 g/cm3

If there is any uncertainty about the numerical value of the density used to calculate the thickness in micrometres from the surface density in milligrams per square centimetre, the density value used should be stated.

11. DETERMINATION OF MASS OF COATING ON WIRE

(BELOW 5 mm IN NOMINAL DIAMETER) BY VOLUMETRIC METHOD

11.1 Outline of the Method

The volumetric method. of determining the mass of coating depends on the fact that a metal dissolved in acid always releases a quantity of hydrogen in strict proportion to the amount of metal dissolved.

11.2 Reagents

11.2.1 Dissolve 20 g of antimony trioxide (Sb2O2) or 32 g of antimony trichloride (SbCl2) in 1000 ml of concentrated hydrochloric acid (sp gr 1.16).

11.2.2 Immediately before test, prepare the stripping solution by adding 5 ml of the solution prepared under 10.1.1 to 100 ml of concentrated hydrochloric acid (sp gr 1·16). Mix well.

11.3 Apparatus

The apparatus should consist of a 100-ml glass burette fitted with a stopcock at the top and the bottom and connected at the bottom with a rubber tube to a reservoir. The apparatus set up for the commencement of a test is shown in Fig. 1.

11.4 Preparation of Test Piece

Cut accurately a test piece of required length from a sample of wire. The most suitable length of the test piece depends on. the size of the burette, diameter of wire and expected mass of zinc coating. The lengths given below will be found convenient.

| Nominal Diameter of Galvanized Wire (mm) | Length Of the Test Piece (mm) |
| --- | --- |
| Above 0.4 to 1.00 | 300 |
| Above 1.00 to 1.50 | 150 |
| Above 1.50 to 3.00 | 100 |
| Above 3.00 | 50 |

11.5 Cleaning of Test Piece

The test pieces shall be washed with solvent naphtha, trichloroethylene or any other suitable organic solvent, then with alcohol and finally dried thoroughly.

11.6 Procedure

11.6.1 Pour the acid reagent into the reservoir so that it completely fills the burette leaving a small portion in the reservoir when in the elevated position,

11.6.2 To carry out adjust the height of the reservoir C so that the acid reagent just fills the burette up to the stopcock A with the bottom stopcock B closed, Drop the sample of the specified length into the burette and close the upper stopcock A immediately,

11.6.3 The zinc coating rapidly dissolves and liberates hydrogen and the test is continued until evolution of hydrogen, but for a few fine bubbles, has ceased. Lift the reservoir C from its supporting ring and place alongside the burette until the levels of the acid reagent in the burette and the reservoir are equal as shown in Fig, 2, when the volume of hydrogen is read off on the burette scale.

11.6.4 When the test is concluded; open the upper stopcock A and draw all acid reagent from the burette by lowering the reservoir C to a position below lower stopcock B. Open lower stopcock B to eject the test piece,

11.6.5 This method is usually limited to wires of maximum diameter. 5 mm as with larger diameters, problems of test piece preparation and damage to the glass burette may be introduced. However, where long test pieces are necessary, rapid entry into the burette may be difficult and it may be more convenient to drop the short piece simultaneously through the stopcock.

11.6.6 Wash the stripped wire, wipe it dry and measure the diameter to 0.01 mm at right angle to each other of the same location to obtain the average value.

11.7 Calculation

Mass of coating in g / m2 = (v × f) / ( d × l)

where

v = corrected volume of hydrogen in ml that would be displaced at 0°C and 760 mm mercury pressure,

f = 929. It is a factor obtained on the basis that 343 ml of hydrogen are liberated at 0°C and 760 mm mercury

pressure by one gram of zinc,

d = the diameter in mm of stripped wire, and

l = the length of the test piece in mm.

Annex A

(informative)

Reagents for selective dissolution of metal layers

The stripping methods cited in Table A.1 are described in specifications, in the open literature, or have been used routinely by at least one laboratory.

With many of the reagents given in Table A.1, there may be some dissolution of the layer other than the one being stripped. Often the dissolution is not significant, but the possibility should be tested for as described in 9.5.2 and 9.5.3.

Dissolution is carried out at room temperature unless otherwise indicated. All test pieces are rinsed and dried before weighing.

Table A.1 — Reagents for selective dissolution of metallic and other inorganic coatings using both chemical and electrochemical methods

| Coating | Substrate | Reagentsa | Comments |
| --- | --- | --- | --- |
| Aluminium | Steel | (1) 20 parts by mass NaOH + 80 parts water (2) concentrated HCl | See ASTM A428M-10(2014) Immerse for a few minutes (avoid a longer time) at about 90 °C. While rinsing, scrub with a sponge to remove loose material. Drain off water, immerse for 3 s in concentrated HCl at room temperature, scrub again in running water, repeat the entire process until there is no visible reaction in HCl. Two or three cycles are required normally. |
| Cadmium | Steel | 300 g/l NH4NO3 | See ISO 2082:2017. Immerse. |
| Cadmium | Steel | 200g Sb2O3 in 1l concentrated HCl | See Reference [16]. Immerse till evolution of gas practically stops |
| Cadmium | Steel | 20g Sb2O3 in 800 ml concentrated HCl + 200 ml of water | Immerse till evolution of gas practically stops |
| Cadmium | Steel | 5 % (NH4)2S2O8 + 10 % by volume of concentrated NH4OH solution | See Reference [16]. Immerse. |
| Chromate | Aluminium | (1) (1) NaNO2 (2) 1 part by volume water + 1part concentrated HNO3 | See ASTM B449-93 (2015). Immerse in molten NaNO2 at 326 °C to 354 °C for 2 min, rinse in cold water, then in reagent (2) for 30 s at room temperature. |
| Chromate (aged) | Aluminium and its alloys | (1) 98 % NaNO3 + 2 % NaOH solution (2) (2) 1 part by volume 65 % to 70 % mass fraction HNO3 + 1 part water | See ISO 3892:2000. Immerse in (1) for 2 min to 5 min at 370 °C to 500 °C (some coatings may require the higher temperature). Rinse in water, immerse in (2) for 15 s to 30 s at room temperature. |
| Chromate (fresh) | Aluminium alloys | 1 part by volume water + 1 part 65 % to 70 % mass fraction HNO3 | See ISO 3892:2000. Immerse for 1 min at room temperature within 3 h of application of coating. |
| Chromate (aged and fresh) | Aluminium alloys | (1) 500 ml 1 % H2SO4 (2) (NH4)2S2O8 | See EN 12487:2007. Immerse in (1) for 10 min at boiling point, evaporate to about 50 ml. Treat with (2) (concentration not critical) to oxidize Cr (III) to Cr (VI). Determine photometrically at wavelength (λ) = 445nm |
| Chromate | Tin or zinc | (1) 100g KNO3 + 100 g KCl in 1 l of water (2) 100 g NaCl or KCl in 1 l of water | Immerse chromates on tin in (1), rinse, dry and determine gravimetrically or volumetrically. Immerse chromates on zinc in (2), rinse, dry and determine gravimetrically or volumetrically. |
| Chromium | Nickel or steel | 12 g/l NaOH | See Reference[14] Chromium dissolve anodically at about 20Ma/cm2. |
| Copper | Zinc alloys | 1 part of concentrated HCl+ 4 parts of water | Dissolves zinc alloy substrate. Cool initial reaction to prevent dissolution of copper. |
| Gold | Steel, copper, nickel or Fe-Ni-Co | 1 to 3 parts by volume water + 1part concentrated HNO3 | Substate dissolved by immersion. Heat as required. Keep free of halides. Nickel may passivate - make contact with nickel wire to increase area of nickel. |
| Lead-tin alloys | Steel |  | See “terne plate”. |
| Nickel | Brass | 90% H2PO4 | Immerse at 180 °C to 190 °C, do not add water. 2,5 μm nickel dissolve in about 10 min |
| Nickel or nickel over copper | Zinc Alloys | 1 part concentrated HCl + 4 parts water | See Reference [15]. Dissolves zinc alloy substrate. Cool initial reaction to prevent dissolution of copper. Check for dissolution of nickel. |
| Phosphate (amorphous) | Aluminium and its alloys | 1 part by volume water + 1 part 65 % to 70 % mass fraction HNO3 | See ISO 3892:2000. Immerse for 1 min at room temperature |
| Phosphate (Crystalline) | Aluminium and its alloys | 65 % mass fraction HNO3 + 35 % mass fraction H2O | See ISO 3892:2000. Immerse 5 min at 75 °C, or 15 min at room temperature. |
| Phosphate (zinc base) | Steel | 100 g/l NaOH + 90 g/l EDTAb tetra-sodium salt + 4 g/l triethanolamine | See ISO 3892:2000. Immerse for 5 min at 70 °C (±) 5 ⁰ |
| Silver | Nickel Brass | 19 parts by volume concentrated H2SO4 + 1 part by volume concentrated HNO3 | See Reference [13]. Immerse at 80 °C. |
| Silver | Copper alloys | (1) 19 parts by volume concentrated H2SO4 + 1 part by volume concentrated HNO3 (2) concentrated H2SO4 | Immerse at 60 °C to 70 °C until silver dissolves, dip in concentrated H2SO4 rinse. |
| Terne Plate | Long terne sheet(steel) | (1) 100 g/l NaOH (2) 1 volume concentrated HCl + 3 volumes water | Strip anodically in NaOH solution, 77⁰ C to 88⁰ C, 12 A/dm2, reverse current 5s to 15s, rinse, dip in HCl solution for 1s to 2 s, rinse, dip in HCl solution for 1s to 2s, rinse. |
| Terne Plate | Long terne sheet(steel) | 200 g/l AgNO3 | Immerse, silver replaces terne metal, remove by scrubbing in water and examine for residual terne metal. |
| Tin | Copper alloys | concentrated HCl | See ISOP 2081:2018 and BS 1872:1984 Immerse and simmer at 95⁰ C or higher until tin is dissolved. |
| Tin | Steel | 40% NaOH | Immerse and heat until evolution of gas stops. Used routinely in one or more laboratories. |
| Tin | Steel | 20g Sb2O3 in 1 l concentrated HCl | See ISO 2081:2018 and [17]. Immerse until 1 min after evolution of gas stops. |
| Tin- lead alloy | Copper | 10ml concentrated HNO3 + 15g urea + 10 ml H2O2 (10 volume) + 80 ml water | See Reference [18]. Alloy dissolves at about 0,1 μm/min. Copper dissolves at about 0,5 mg dm–2 min–1. |
| Tin- lead alloy | Copper and copper alloys | 50 ml H2O2 6% mass fraction + 50 ml fluoboric acid (HBF4) 40 % mass fraction | See ISO 7587:1986. Immerse in freshly prepared solution. |
| Tin- lead alloy | Nickel and steel | 20 g/l Sb2O3+ 1 000 ml concentrated HCl | See ISO 7587:1986. Immerse. |
| Tin- nickel alloy | Copper and copper alloys | concentrated H3PO4 | See BS 3597:1984. Immerse at 180 °C to 200 °C. |
| Zinc | Steel | 20 g Sb2O3+ 50 g SnCl2 in 100 g concentrated HCl | See ISO 8407:2009. Immerse in solution. Keep below 38 °C until violent evolution of hydrogen has stopped and only a few bubbles are being evolved. |
| Zinc | Steel | 20 g Sb2O3+ 800 ml concentrated HCl + 200 ml water | Immerse until effervescence ceases. |
| Zinc | Steel | 3.5 g hexamethylene tetramine in 500 ml concentrated HCl + water to 1 l | See ISO 1460. Immerse in solution until hydrogen evolution ceases and the coating is dissolved, brush off loose deposit, rinse in water. |
| Zinc | Steel | 5 g (NH4)2S2O8+ 10 ml NH4OH (ρ20 = 0,880) + 90 ml water | Immerse |
| Zinc | Steel | 10 ml formaldehyde 30 % mass fraction + 500 ml concentrated HCl + 500 ml water | See ISO 2081: 2018 Immerse |
| Zinc | Steel | 300 g/l NH4NO3 | See ISO 2081: 2018 Immerse |
| Zinc | Steel | 500 g concentrated HCl + 1 g prop-2-yn-1-ol (C3H4O) + 500 ml water | Immerse |

a The relative densities at 20 °C (ρ20) of the acids referred to in this table are as follows:

— hydrochloric acid HCl, 1.18;

— nitric acid HNO3, 1.42;

— phosphoric acid H3PO4, 1.75;

— sulfuric acid H2SO4, 1.84.

b EDTA = ethylene diamine tetra acetic acid

Bibliography

[1] ISO 1460, Metallic coatings — Hot dip galvanized coatings on ferrous materials — Gravimetric determination of the mass per unit area

[2] ISO 2081:2018, Metallic and other inorganic coatings — Electroplated coatings of zinc with supplementary treatments on iron or steel

[3] ISO 2082:2017, Metallic coatings — Electroplated coatings of cadmium with supplementary treatments on iron or steel

[4] ISO 2093:1986, Electroplated coatings of tin — Specification and test methods

[5] ISO 3892:2000, Conversion coatings on metallic materials — Determination of coating mass per unit area — Gravimetric methods

[6] ISO 7587:1986, Electroplated coatings of tin-lead alloys — Specification and test methods

[7] ISO 8407:2009, Corrosion of metals and alloys — Removal of corrosion products from corrosion test specimens

[8] ASTM A428M-10(2014), Standard Test Method for Weight (Mass) of Coating on Aluminium-Coated Iron or Steel Articles

[9] ASTM B449-93 (2015), Standard Specification for Chromates on Aluminium

[10] BS 1872:1984, Specification for electroplated coatings of tin

[11] BS 3597:1984, Specification for electroplated coatings of 65/35 tin/nickel alloy

[12] EN 12487:2007, Corrosion protection of metals — Rinsed and non-rinsed chromate conversion coatings on aluminium and aluminium alloys

[13] United States Standard RR-T-51 D, Tableware and Flatware — Silverplated

[14] Brenner